Benzo[1,2-d:4,5-d′]bisthiazole fluorophores for luminescent solar concentrators: synthesis, optical properties and effect of the polymer matrix on the device performances

Costanza Papucci,a,b,c Alessio Dessì,a Carmen Coppola,b,d Adalgisa Sinicropi,a,b,d Greta Santi,e Mariangela di Donato,a,f Maria Taddei,a,f Paolo Foggi,f,g,h Lorenzo Zani,a Gianna Reginato,a Andrea Pucci,*e Massimo Calamante,*a,c and Alessandro Mordini,a,c

a Institute of Chemistry of Organometallic Compounds (CNR-ICCOM), Via Madonna del Piano 10, 50019 Sesto Fiorentino, Italy;

b Department of Biotechnology, Chemistry and Pharmacy, University of Siena, Via A. Moro 2, 53100, Siena, Italy;

c Department of Chemistry “U. Schiff”, University of Florence, Via della Lastruccia 13, 50019 Sesto Fiorentino, Italy;

d CSGI, Consorzio per lo Sviluppo dei Sistemi a Grande Interfase, Sesto Fiorentino 50019, Italy;

e Department of Chemistry and Industrial Chemistry, University of Pisa, Via Giuseppe Moruzzi 13, 56124 Pisa, Italy;

f LENS, European Laboratory for Non-Linear Spectroscopy, via N. Carrara 1, Sesto Fiorentino  50019, Italy.

g Department of Chemistry, Biology and Biotechnology, University of Perugia, via Elce di Sotto 8, 06123 Perugia, Italy

hINRIM (Istituto Nazionale di Scienza Metrologica), Strada delle Cacce 91, 10135 Torino, Italy

ABSTRACT

Three new fluorophores (BBT2-4) with a D-A-D structure characterised by the common benzo[1,2-d:4,5-d′]bisthiazole (BBT) as acceptor core (A) and different donor groups (D) were designed and synthesised for use in thin-film luminescent solar concentrators (LSC). The optical and spectroscopic properties of the new dyes were analysed both in solution (toluene) and in polymeric films, using static and time-resolved spectroscopies. All the prepared molecules showed intense emissions between 460 and 550 nm with large Stokes shift (> 50 nm), moderate-to-good fluorescence quantum yields (Φf) both in toluene solution (18-73%) and in poly(methyl methacrylate) (PMMA) films (10-52%) and good optical efficiencies (5.8-7.5%) as LSC. Transient absorption spectroscopy (TAS) studies highlighted that higher  Φf were related to long excited-state lifetimes and that such properties were critically dependent on the polarity of the surrounding environment. Notably, homogeneous BBT4 dispersions into the less polar poly(benzyl methacrylate) (PBzMA) and poly(cyclohexyl methacrylate) (PCMA) polymeric matrices showed higher Φf (52.6% and 65.6%, respectively) than those gathered from PMMA films. Accordingly, BBT4/PCMA films revealed significant optical efficiency of 9.0% as LSC, which was comparable to that provided by the state-of-art fluorophore Lumogen Red 305 (10.1%).

# Introduction

Silicon-based solar cells are still the main photovoltaic (PV) devices used worldwide to exploit renewable energy sources in an effort to reduce fossil fuels consumption. Due to their high efficiency and light-harvesting capability, such cells are indeed the most used devices for the conversion of solar energy into electricity. Nonetheless, in search of more flexible and efficient options, several alternative technologies have been developed in the last 30 years, such as thin-film solar cells[1,2], DSSCs[3,4] and perovskite solar cells[5,6]. In addition, luminescent solar concentrator (LSC) technology has recently received considerable attention. According to the first definition of Weber and Lambe[7], a LSC consists of a polymeric panel doped with a high optical efficiency fluorophore, which can absorb sunlight and emit it in a specific spectral range. Due to the different refraction index of the polymeric material and air,[8] most of the emitted light is concentrated at the edges of the panel, where a PV cell can be located. Being the light concentrated, the surface of the PV cell can be very small, allowing to use materials different from silicon. Moreover, the final device is coloured and not opaque, thus allowing easy integration in buildings, e. g. in windows and onto rooftops. Despite these advantages, the LSC technology still presents some drawbacks limiting its photovoltaic efficiency. A key point to performance increase is to develop new emitters and in particular, to design suitable fluorophores having a wide absorption range (between 450 and 700 nm, areas of maximum intensity of the spectrum of solar radiation reaching the earth), a high fluorescence quantum yield, a large Stokes displacement, with limited overlap between absorption and emission spectra, good solubility in the host matrix and long-term stability.

Various materials have been developed as emitters, such as quantum dots[9],[10],[11], inorganic fluorophores (rare earths complexes[12]), and small organic molecules like perylene diimides[13], BODIPY oligomers[14], benzothiadiazoles[15],[16,17] and diketopyrrolopyrroles dyes[18].

Recently, we proposed new fluorophores for LSC applications based on the benzo[1,2-d:4,5-d′]bisthiazole (BBT) heterocyclic core and characterised by a donor-acceptor-donor (D-A-D) structure[19] (Figure 1). In particular, dye BBT1 was decorated with triphenylamines as donor groups, and thiophene rings were added between the core and the donor groups to increase the conjugation, inducing a red-shift of the absorption and emission spectra. Such a dye, when integrated into poly(methyl methacrylate) (PMMA) films at different concentrations, gave a maximum optical efficiency of 6.4%, close to the value of 7.2% measured, in the same conditions, for the reference standard Lumogen Red 305 (LR 305).

Figure 1.  Structures of LR 305 and BBT1.

An important feature of the new fluorophore BBT1 was its large Stoke shift of 94 nm in ethanol (0.48 eV), ensuring a small overlap between the absorption and the emission bands, thus minimising the self-absorption phenomena. This could enable the use of this type of luminophore in devices with a large surface area without a great loss in optical efficiency, which instead occurs when LR 305 is employed[20].

Starting from the above-mentioned results, we decided to extend our study to a new series of BBT-derivatives still having a D-A-D design but carrying different donor groups. The aim was to obtain new fluorophores with absorption and emission in different spectral ranges, to tune the colour of the resulting poly(methyl methacrylate) (PMMA) films and, at the same time, to increase or, at least, maintain the optical characteristics suitable for LSC application (i.e., quantum yield, Stokes shift, optical efficiency). In addition, expanding our previous studies, we wanted to combine the computational characterisation of the dyes with appropriate transient absorption spectroscopy (TAS) studies, with the aim to investigate the dynamics of light absorption and emission processes, both in solution and in the solid state, and correlate them with the optical performances of the devices.

The new dyes have been synthesised and completely characterised both in solution and as dispersion in three different polymeric matrices, namely PMMA, poly(benzyl methacrylate) (PBzMA) and poly(cyclohexyl methacrylate) (PCMA) with the aim also to test the effect of the less polar lateral substituent (i.e. benzyl and cyclohexyl compared to the traditional methyl ester group in PMMA) on the optical features of the derived films.

Their computational characterisation and TAS investigation have been carried out, and the prepared thin-film LSC devices were eventually characterised in terms of their photovoltaic performances.

# Experimental Section

## General Remarks

All commercially available compounds were purchased from Merck KgaA, Fluorochem Ltd. and T.C.I. Co. Ltd., and were used without further purification unless stated otherwise. Anhydrous toluene and N,N-dimethylformamide (N,N-DMF) were obtained after drying with a PureSolv Micro apparatus (Inert). Tetrahydrofuran was dried by distillation on metallic sodium using benzophenone as indicator until the characteristic blue colour of in situ-generated sodium diphenyl-ketyl radical was found to persist. Diisopropylamine was distilled under inert atmosphere and kept over KOH. Poly(methyl methacrylate) (PMMA, Aldrich, Mw = 350,000 g/mol, Tg = 105 °C) , Poly(benzyl methacrylate) (PBzMA, Aldrich, Mw = 100,000 g/mol, Tg = 54 °C) and Poly(cyclohexyl methacrylate) (PCMA, Aldrich, Mw = 65,000 g/mol, Tg = 104 °C) were used as received. Organometallic reactions were carried out under dry nitrogen using Schlenk techniques. Solvent degassing was carried out according to the “freeze-pump-thaw” method. The temperature of –78 °C was obtained with a liquid N2/acetone cooling bath. Reactions were monitored by TLC on Kieselgel 60 F254 (Merck) aluminium sheets, and the products were visualised by exposing the plate to UV light or by staining it with KMnO4 solution. Flash column chromatography[21] was performed using Merck Kieselgel 60 (300–400 mesh) as the stationary phase. 1H-NMR spectra were recorded at 200–400 MHz, and 13C-NMR spectra were recorded at 50.3–100.6 MHz, respectively, on Varian Gemini/Mercury/INOVA series instruments. Chemical shifts (δ) are reported in parts per million (ppm) and are referred to the residual solvent peak (CDCl3, δ = 7.26 ppm for 1H-NMR and δ = 77.0 ppm for 13C-NMR; CD2Cl2 δ = 5.32 ppm for 1H-NMR and δ = 53.84 ppm for 13C-NMR; THF-d8 δ = 3.58, 1.73 ppm for 1H-NMR and δ = 67.57, 25.37 ppm for 13C-NMR), while coupling constants (J) are reported in Hz. GC/MS analyses of species with MW lower than 400 g/mol were performed using a Shimadzu QP505A gas-chromatograph. ESI-MS spectra were obtained by direct injection of the sample solution using a Thermo Scientific LCQ-FLEET instrument, while HRMS spectra were measured using a Thermo Scientific LTQ Orbitrap (FT-MS) instrument (carried out at the Interdepartmental Center for Mass Spectroscopy of the University of Florence, CISM); both are reported in the form m/z. UV/Vis spectra in solution were recorded with a Varian Cary 4000 spectrometer, and fluorescence spectra in solution were recorded with a Varian Eclipse instrument, irradiating the sample at the wavelength corresponding to maximum absorption in the UV spectrum.

UV-Vis absorption spectroscopy on polymer films was performed at room temperature by using an Agilent Cary 5000 spectrophotometer. Fluorescence spectra on polymer films were measured at room temperature with a Horiba Jobin–Yvon Fluorolog®-3 spectrofluorometer equipped with a 450W Xenon arc lamp and double-grating excitation and single-grating emission monochromators. The emission quantum yields (Φf) were determined by using a 152 mm diameter “Quanta-φ” integrating sphere, coated with Spectralon® and following the procedures reported earlier.[22–24] The optical microscope analysis was accomplished on a SMZ-168-BLED Motic microscope and the images collected by a 12MP digital camera with a ƒ/1.8 aperture. The concentration factors and the optical efficiencies of the LSC were obtained by using a solar simulator (ORIEL® LCS-100 solar simulator 94011A S/N: 322, AM1.5G std filter: 69 mW/cm-2 at 254 mm) and a PV cell (IXYS SLMD121H08L mono solar cell 86×14 mm, Voc = 5.04 V, Isc = 50.0 mA, FF > 70%, η = 22%)[25–28] connected to a precision source/measure unit (Keysight Technologies B2900 Series). The PV cell is masked with black tape to match LSC edge (50 mm x 3 mm) so that limiting the stray light to negligible levels. Silicon was used to grease the LSC edge. The other three edges of the LSC were covered with a reflective aluminium tape.

The optical efficiency ηopt was determined from the concentration factor (C), i.e. the ratio between the maximum power measured for the cell over the LSC edge (PLSC) and that of the bare cell when perpendicular to the light source (PSC):

ηopt=PLSCPSC∙G	                              (1)

where G is the geometrical factor (G = 16.6) that is the ratio between the area exposed to the solar simulator and the collecting area by the PV cell. A white backscattering layer (ERGA TAPES Srl Microcellular MCPET reflective sheet) was placed beneath the LSC with an air gap of about 2.5 mm during the PLSC measurements. The reported ηopt values were calculated as the average of three distinct measurements on identical LSC samples.

## Synthesis

### Synthesis of 3-hexyl-2-thiophenecarboxaldehyde (2).

In a Schlenk tube, under an inert atmosphere of N2, to a suspension of Mg° (370 mg, 15.2 mmol, 2.5 eq, preactivated in a solution of HCl 1 M) in dry THF (12 mL), one drop of 1,2-dibromoethane and then 2-bromo-3-hexylthiophene 1 (1.5 g, 6.1 mmol, 1.0 eq) were added. The mixture was stirred under reflux for 2 h. Then the mixture was cooled first to room temperature, then to −78°C. N,N-DMF (2.36 mL, 30.5 mmol, 5.0 eq) was added dropwise to the solution. The mixture was warmed slowly until it reached room temperature and stirred for 12h, then a saturated aqueous solution of NH4Cl (10 mL) was added under vigorous stirring and the mixture was extracted with diethyl ether (2 × 15 mL). The organic phase was washed with H2O (12 mL) and brine (12 mL) and dried on Na2SO4. The crude product (1.090 g, 91%) was directly used in the next step without further purification. Spectroscopic data are in agreement with those reported in the literature[19]. 1H NMR (400 MHz, CDCl3): δ = 10.04 (d, J = 0.9 Hz, 1H), 7.64 (dd, J1 = 5.0 Hz, J2 = 0.9 Hz, 1H), 7.00 (d, J = 5.0 Hz, 1H), 2.96 (t, J = 7.4 Hz, 2H), 1.68–1.62 (m, 2H), 1.40–1.27 (m, 6H), 0.88 (t, J = 8.0 Hz, 3H) ppm. 13C NMR (100 MHz, CDCl3): δ = 182.2, 152.9, 137.6, 134.4, 130.7, 31.5, 31.4, 28.9, 28.5, 22.5, 14.0.

### 2,6-Bis(3-hexylthiophen-2-yl)benzobisthiazole (4).

In a Schlenk tube, aldehyde 2 (1.09 g, 5.55 mmol, 2.5 eq) was dissolved in N,N-DMF (32 mL). 2,5-diamino-1,4-benzenedithiol dihydrochloride 3 (544 mg, 2.22 mmol, 1.0 eq) and ZnCl2 (15 mg, 0.11 mmol, 0.05 eq) were added to the solution. The mixture was stirred in air at room temperature for 16 h obtaining a yellow solid that was recovered by filtration and washed twice with a mixture of petrolium ether and EtOAc (2 × 15 mL) to give product 4 with a yield of 53% (617 mg). Spectroscopic data are in agreement with those reported in literature[19]. 1H NMR (400 MHz, CDCl3): δ = 8.58 (s, 2H), 7.48 (d, J = 5.0 Hz, 2H), 7.06 (d, J = 5.0 Hz, 2H), 3.07 (t, J = 4.0 Hz, 4H), 1.81–1.69 (m, 4H), 1.30–1.54 (m, 12H), 0.80–0.95 (m, 6H) ppm. 13C NMR (100 MHz, CDCl3): δ = 162.1, 149.4, 146.0, 134.1, 131.1, 130.4, 129.4, 114.3, 31.6, 30.3, 30.2, 29.3, 22.6, 14.1 ppm. ESI-MS: m/z = 525.3 [M + H]+.

### 2,6-Bis(5-bromo-3-hexylthiophen-2-yl)benzobisthiazole (5).

In a round-bottom flask, compound 4 (930 mg, 1.77 mmol, 1.0 eq) was dissolved in a mixture of CHCl3 and acetic acid (2:1 v/v) (40 mL). The solution was cooled at 0°C and NBS (1.263 g, 7.09 mmol, 4.0 eq) was added. The mixture was stirred at room temperature in the dark for 72 h. Then water (30 mL) was added and the organic phase was extracted with CHCl3 (2 × 30 mL). The organic phase was washed with water (20 mL) and brine (20 mL) and dried on Na2SO4. The solvent was evaporated and the residue recrystalized from ethyl acetate to give compound 5 as a yellow solid with a yield of 98% (1.16 g). 1H NMR (400 MHz, CDCl3 + 10 % v/v TFA-d): δ = 8.81 (s, 2H), 7.28 (s, 2H), 3.00 (t, J = 7.9 Hz, 4H), 1.75–1.85 (m, 4H), 1.44–1.54 (m, 4H), 1.30–1.39 (m, 8H), 0.91 (t, J = 6.9 Hz, 6H) ppm. 13C NMR (100 MHz, CDCl3 + 10 % v/v TFA-d): δ = 165.8, 155.6, 140.1, 135.7, 131.7, 127.4, 124.7, 112.6, 31.4, 31.2, 29.4, 29.1, 22.4, 13.8 ppm. ESI-MS: m/z = 685.3, 683.2, 681.2 (1:2:1) [M + H]+.

### Synthesis of BBT2.

In a microwave tube, Pd2(dba)3 CHCl3 (7.6 mg, 0.007 mmol, 0.05 eq) was mixed with Xantphos (17.5 mg, 0.015 mmol, 0.1 eq) under stirring for 20 minutes in dry toluene (3 mL). In a Schlenk tube, 9H-carbazole 6 (149 mg, 0.3 mmol, 2.0 eq) and tBuONa (42 mg, 0.44 mmol, 3.0 eq) were dissolved in MeOH (0.5 mL). The resulting solution was transferred in the microwave tube and compound 5 (100 mg, 0.15 mmol, 1.0 eq) was then added. The mixture was stirred for 30 minutes at room temperature and then heated in the MW reactor at 70°C, for 35 minutes. The mixture was cooled to room temperature obtaining a yellow solid precipitate. The solid was recovered by filtration and washed with cold toluene (10mL), water (2x10mL) and then dried under vacuum, giving BBT2 as yellow amorphous solid (150 mg, yield >99%). 1H NMR (400 MHz, THF-d8): δ = 8.62 (s, 2H), 8.16 (d, J = 8.0 Hz, 4H), 7.71 (d, J = 8.2 Hz, 4H), 7.47 (dt, J1 = 7.0, J2 = 1.2, 4H), 7.36 (s, 2H), 7.34-7.29 (m, 4H), 3.28-3.22 (m, 4H), 1.96-1.87 (m, 4H), 1.65-1.56 (m, 4H), 1.50-1.35 (m, 8H), 0.95 (t, J = 7.0, 6H). 13C NMR (100 MHz, THF-d8): δ = 152.1, 145.5, 142.3, 142.2, 135.8, 129.9, 128.6, 127.4, 125.1, 122.1, 121.2, 115.9, 115.8, 111.3, 32.8, 31.5, 31.3, 30.8, 23.7, 14.6. HRMS: calculated for C52H47N4S4: 855.2683. Found: 855.2703 [M+H]+.

### Synthesis BBT3.

In a microwave tube, Pd2(dba)3 CHCl3 (4.0 mg, 0.0038 mmol, 0.05 eq) was mixed with Xantphos (4.4 mg, 0.0075 mmol, 0.1 eq) under stirring for 20 minutes in dry toluene (3 mL). In a Schlenk tube, boronic ester 7 (59 mg, 0.15 mmol, 2.0 eq) and KF (13 mg, 0.225 mmol, 3 eq) were dissolved in MeOH (0.5 mL). The resulting solution was transferred in the microwave tube and compound 5 (50 mg, 0.075 mmol, 1.0 eq) was then added. The mixture was stirred for 30 minutes at room temperature and then heated in the MW reactor at 70°C, for 35 minutes. After cooling to room temperature the solvent was evaporated and the crude was purified by flash column chromatograpy (SiO2, petroleum ether / DCM / tol 6:2:1) to give compound BBT3 (33.4 mg, 43%) as a pale orange solid. 1H NMR (400 MHz, THF-d8): δ = 8.58 (s, 2H), 8.14 (d, J=7.8Hz, 4H), 7.97 (d, J=7.8Hz, 4H ), 7.64 (s, 2H), 7.56 (d, , J=8.6Hz, 4H), 7.46-7.40 (m, 4H), 7.23 (t, , J=7.4Hz, 4H), 6.83 (d, , J=8.6Hz, 4H), 3.21-3.18 (m, 4H), 1.60-1.30 (m, 16H), 0.94 (t, J = 8.0 Hz, 6H) ppm. 13C NMR (100 MHz, THF-d8): δ = 152.2, 147.2, 146.1, 145.1, 140.7, 139.9, 135.7, 133.1, 132.8, 132.5, 129.8, 129.3, 127.9, 125.4, 123.8, 122.9, 118.1, 115.8, 32.9, 31.4, 31.3, 30.5, 23.7, 14.6.  HRMS: m/z calculated for C64H54N4S6: 1070.2673. Found: 1070.2672 [M·]+.

### Synthesis of BBT4.

In a microwave tube, Pd2(dba)3 CHCl3 (4.0 mg, 0.0038 mmol, 0.05 eq) was mixed with Xantphos (4.4 mg, 0.0075 mmol, 0.1 eq) under stirring for 20 minutes in dry toluene (3 mL). In a Schlenk tube, boronic ester 8[51] (63 mg, 0.15 mmol, 2.0 eq) and KF (13mg, 0.225 mmol, 3 eq) were dissolved in MeOH (0.5 mL). The resulting solution was transferred in the microwave tube and compound 5 (50 mg, 0.075 mmol, 1.0 eq) was then added. The mixture was stirred for 30 minutes at room temperature and then heated in the MW reactor at 70°C, for 35 minutes. After cooling to room temperature, the solvent was evaporated and the crude was purified by flash column chromatograpy (SiO2, petroleum ether / DCM 3:1), to give compound BBT4 (57.6 mg, 69%) as an orange solid. 1H NMR (400 MHz, THF-d8): δ = 8.49 (s, 2H), 7.37 (d, J=2.1 Hz, 2H), 7.34 (d, J = 8.8 Hz, 4H), 7.29 (s, 2H), 7.21 (d, J1 = 8.8 Hz, 4H), 6.98 (dd, J1 = 7.2 Hz, J2 = 2.0 Hz, 2H), 6.85-6.77 (m, 4H), 6.21 (d, J1 = 8.2, 2H), 6.18 (dd, J1 = 7.2 Hz, J2 = 2.0, 2H), 3.89 (s, 6H), 3.12-3.08 (m, 4H), 1.56-1.51 (m, 4H), 1.42–1.36 (m, 4H), 1.28-1.27 (m, 8H), 0.89 (t, J = 8.1 Hz, 6H) ppm. 13C NMR (100 MHz, THF-d8): δ = 161.5, 160.9, 152.2, 147.1, 145.8, 145.1, 135.5, 134.0, 133.1, 128.9, 127.9, 127.4, 127.1, 125.3, 124.3, 123.5, 120.1, 117.1, 116.9, 116.8, 56.0, 32.8, 32.7, 31.3, 30.6, 23.7, 14.6.(some quaternary carbon signal missing due to low solubility). HRMS: m/z calculated for C66H59N4O2S6: 1131.2962. Found: 1131.2989 [M+H]+.

## Transient Absorption Spectroscopy

Ultrafast transient absorption spectra of all samples have been measured on a system consisting of a home-built Ti:sapphire laser oscillator and regenerative amplifier system (Amplitude Pulsar) which produced 80 femtoseconds pulses at 810 nm with an average output power of 450 to 500 mW. Excitation pulses at 400 nm were obtained by the second harmonic generation of the fundamental laser output in a 2 mm thick BBO crystal. For all measurements, the pump beam polarization was set at the magic angle with respect to the probe beam by rotating a /2 plate to exclude rotational contributions to the transient signal[29,30].

The excitation powers were on the order of 50 to 100 nJ. The probe pulses were generated by focusing a portion of the 800 nm radiation beam on a 3 mm thick CaF2 window. The time delay between pump and probe pulses was introduced by sending the portion of 800 nm light used for probe generation through a motorised stage. After passing through the sample, the white light probe was sent to a flat field monochromator coupled to a home-made CCD detector. For samples in solution measurements were performed in a quartz cell (2 mm thick) mounted on a movable stage in order to refresh the solution and avoid undesired photochemical degradation of the sample. In the case of samples dispersed in PMMA, the polymeric films were directly mounted on the same motorised stage used for liquid samples.

Analysis of the transient data was performed applying Singular Value Decomposition (SVD)[31] and global analysis[32], using the software GLOTARAN[33]. Global analysis allows the simultaneous fit at all the measured wavelengths with a combination of exponential decay functions and retrieves the kinetic constants describing the dynamic evolution of the system and the corresponding spectral component, called Evolution Associated Difference Spectra (EADS). A linear decay kinetic scheme was employed for data analysis.

## Computational details

Molecular and electronic properties of compounds BBT2, BBT3 and BBT4 have been computed via DFT[34–36] and time-dependent DFT (TD-DFT)[37,38] methods, using Gaussian 09, Revision C.01 suite of programs.[39] The S0 optimised geometries of compounds BBT2-4 were obtained at B3LYP[40,41]/6-31G* level of theory in vacuum, as well as the ground-state electron density delocalisation and the energy of FMOs in solvent (toluene), while the S1 optimised geometries were computed at TD-CAM-B3LYP[42]/6-31G* level of theory. The UV-Vis spectroscopic properties of the analysed compounds, including absorption (λmaxabs) and emission maxima (λmaxemi), vertical excitation (Eexc) and emission (Eem) energies, oscillator strengths (f) and composition (%) in terms of molecular orbitals for the lowest singlet-singlet excitations and the singlet-singlet emissions, S0S1 and S1S0 respectively, in toluene and PMMA, have been computed on the minimised structures at TD-MPW1K[43]/6-311+G(2d,p) level of theory. Solvent effects have been included by using the polarisable continuum model (PCM) and, in the case of the emission maxima, using the Linear-Response implementation (LR-PCM).[44]

## LSC preparation

Polymer thin films containing the selected fluorophore were prepared by pouring 1.5 mL of toluene (Sigma-Aldrich, HPLC Plus, for HPLC, GC, and residue analysis, ≥99.9%) solution containing about 60 mg of the polymer and different concentrations (0.2-1.8 wt.%) of the fluorophore on a 50×50×3 mm optically pure glass substrate (Edmund Optics Ltd BOROFLOAT window 50×50 TS). The amount of fluorophore was taken from a mother solution at a concentration of 1.5 mg/mL. The glass slides were cleaned with chloroform and immersed in 6 M HCl for at least 12 h and then dried according to previously reported procedures.[24,25,45–48] Fluorophore-doped polymer thin films with a thickness of 25 ± 5 μm (Starrett micrometer) were obtained after complete evaporation of toluene at room temperature under a saturated atmosphere of chloroform (Sigma Aldrich, ACS reagent, ≥99.8%). For absorption and emission spectroscopic characterisation, the polymer films were carefully detached from the glass surface by immersion the LSC in water and then stored in a desiccator.

# Results and Discussion

We designed three new luminophores characterised by the same BBT heterocyclic core employed in the past[19], but symmetrically decorated with 9H-carbazole (BBT2), 10-phenyl-10H-phenothiazine (BBT3) and 10-(4-methoxyphenyl)-10H-phenothiazine (BBT4) as donors (Figure 2).

Figure 2. Structures of the new fluorophores BBT2, BBT3 and BBT4

In particular, the different electron-donor groups were introduced to shift the maximum absorption peaks by affecting the HOMO energy levels, aiming to obtain three materials with different colours. Besides, the more rigid donor groups compared to the triphenylamine present in BBT1 were expected to decrease the energy dissipation through internal conversion and vibrational motions,[49] which should result in a higher fluorescence quantum yield. Finally, alkyl chains were introduced to increase the solubility and possibly favour the fluorophore miscibility into the polymer matrices.

## Computational investigation

A computational investigation based on Density Functional Theory (DFT) and time-dependent DFT (TD-DFT) methods was carried out to rationalise the structural, electronic and photophysical properties of compounds BBT2-4.

The ground (S0) and excited states (S1) optimised geometries of BBT2-4 are shown in Figure 3. S0 geometries of all the luminophores present a planar central scaffold consisting of the BBT core and thiophene rings (dihedral angles ≤ 1°), while a pronounced torsion is found between the donor groups and the thiophene rings (dihedral angles between 24° and 57°). On the other hand, calculated geometries for S1 have smaller torsional angles, thus increasing the overall planarity of the molecules (Figure 3).

Figure 3. Bond lengths (Å) and dihedral angles (degrees) of S0 and S1 (in brackets) optimised geometries of BBT2, BBT3 and BBT4.

TD-MPW1K/6-311+G(2d,p) absorption (λmaxabs) and emission (λmaxemi) maxima, vertical excitation (Eexc) and emission (Eem) energies, oscillator strengths (f) and composition (%) in terms of molecular orbitals for the lowest singlet-singlet excitations (S0S1) and the singlet-singlet emissions (S1S0) in toluene and PMMA of compounds BBT2, BBT3 and BBT4 are shown in Table 1 and Table 2 respectively. The three fluorophores show absorption maxima between 404-441 nm (corresponding to 3.06–2.81 eV), both in toluene and PMMA.

Looking at the DFT orbitals (see Figure S1 and S2, Supporting Information) and, in particular at the frontier molecular orbitals involved in the lowest energy transition (HOMO and LUMO for BBT2 and BBT4, HOMO-2 and LUMO for BBT3), it is evident that the S0→S1 excitation is characterised by an intramolecular charge transfer from the donor to the acceptor group.

BBT2 shows the most blue-shifted computed absorption maximum due to the lower donor character of the carbazole group compared to the phenothiazine group, and its lower conjugation in comparison with BBT3-4. Indeed, a wider angle of approx. 57° between the carbazole group and the thiophene ring is computed. Thanks to the introduction of an additional phenyl ring between the thiophene ring and the phenothiazine donor group, which increases its conjugation (angle of approx. 24°), BBT3 λmaxabs is predicted to be red-shifted by 15 nm in comparison to BBT2. Finally, BBT4 shows the most red-shifted absorption maximum, due to the greater donor strenght of the methoxyphenylphenothiazine (Figure 3).

Table 1. TD-DFT (MPW1K/6-311+G(2d,p)) absorption maxima (λmaxabsin nm), excitation energies (Eexc in eV), oscillator strengths (f) and contributions (%) to the S0 S1 transition in toluene and in PMMA for BBT2, BBT3 and BBT4 compounds.

| Cmpd. | Medium | λmaxabs [nm] | Eexc | f | Transition (%) |
| --- | --- | --- | --- | --- | --- |
| BBT2 | toluene | 404 | 3.06 | 2.20 | 87 (HL) |
|  | PMMA | 404 | 3.06 | 2.20 | 87 (HL) |
| BBT3 | toluene | 419 | 2.95 | 2.78 | 89 (H-2L) |
|  | PMMA | 419 | 2.96 | 2.78 | 89 (H-2L) |
| BBT4 | toluene | 440 | 2.81 | 3.02 | 79 (HL) |
|  | PMMA | 441 | 2.81 | 3.02 | 78 (HL) |

The LR-PCM computed emission maxima (Table 2) fall in the 477-523 nm range, almost coincident both in toluene and PMMA. The computed Stokes shifts (0.47, 0.49 and 0.44 eV for BBT2, BBT3 and BBT4, respectively) look very promising for a potential successful implementation of BBT2, BBT3 and BBT4 in the LSC field.

Table 2.  TDDFT (MPW1K/6-311+G(2d,p)) emission maxima (λmaxemi in nm), emission energies (Eem in eV), oscillator strengths (f) and contributions (%) to the transition S1S0 in toluene and in PMMA for BBT2, BBT3 and BBT4 compounds.

| Cmpd. | Medium | λmaxemi [nm] | Eexc | f | Transition LH (%) |
| --- | --- | --- | --- | --- | --- |
| BBT2 | toluene | 477 | 2.59 | 2.40 | 92 |
|  | PMMA | 477 | 2.60 | 2.40 | 93 |
| BBT3 | toluene | 504 | 2.46 | 2.82 | 93 |
|  | PMMA | 504 | 2.45 | 2.82 | 93 |
| BBT4 | toluene | 521 | 2.38 | 3.18 | 88 |
|  | PMMA | 523 | 2.37 | 3.18 | 88 |

## Synthesis of compounds BBT2-4

The preparation of the three dyes was carried out by applying an easy and flexible synthetic approach, essential to reduce the number and complexity of synthetic operations. To this end, the previously reported synthesis[19] of BBT1 was modified to increase the yields and simplify the purification steps, keeping 2,6-bis(3-hexylthiophen-2-yl)benzo[1,2-d:4,5-d']bis(thiazole) (4) as the common intermediate for the synthesis of the new fluorophores BBT2-4. The new synthetic strategy (Scheme 1) started with the quantitative conversion of commercial bromide 1 into the corresponding aldehyde 2, using a modified Grignard procedure[50].

Scheme 1 Synthesis of BBT derivatives.

Aldehyde 2 was then reacted with commercially available 2,5-diaminobenzene-1,4-dithiol bis-hydrochloride (3) to obtain the BBT tricycle 4. Following a previously reported procedure[19] the reaction was performed using N,N-DMF as solvent under air, at room temperature, and in the presence of ZnCl2 as a Lewis acid, smoothly giving product 4 in 53% yield after crystallisation. Then, dibromo-intermediate 5 was obtained through electrophilic bromination of 4, using a large excess of N-bromosuccinimide (NBS). The reaction was complete after three days at room temperature. The desired compound precipitated from the reaction mixture and was quantitatively recovered by simple filtration, avoiding complex chromatographic purification and recrystallisation. Finally, dibromide 5 was reacted with carbazole 6, using Buchwald-Hartwig conditions, with XantPhos as ligand and tBuONa as base, thus obtaining BBT2 in almost quantitative yield. Otherwise, compounds BBT3 and BBT4 were prepared by performing a Suzuki-Miyaura cross-coupling using boronic esters 7 or 8, respectively, SPhos as the ligand and KF as the base. A lab-scale microwave activation protocol was developed and applied to all cross-coupling reactions, resulting in all cases in a significant reduction of the reaction time, if compared to thermal heating, and in a limitation of side-products, with consequent simplification of the following chromatographic purification. For all coupling reactions, toluene/MeOH (6/1) was the best solvents mixture to ensure a proper dissolution of the starting materials and to absorb microwaves efficiently; Pd2(dba)3 was used as catalyst precursor.

The thermal stability of the dyes were carried out through a thermogravimetric analysis which showed a maintenance of 90-94% of the sample weight up to 200 ° C and 87-89% up to 300 ° C. BBT2 shows slightly faster weight loss than BBT3-4 (Figure S8).

## Spectroscopic characterisation in solution

The optical properties of BBT2-4 were studied in solution by UV-Vis absorption and fluorescence emission spectroscopies. The solvent used was toluene because it could effectively dissolve all compounds and its refractive index (1.496) is similar to that of PMMA (1.491). Relevant data are presented in Table 3 and Figure 4.

Table 3. Spectroscopic properties of compounds BBT2, BBT3 and BBT4 in toluene solution.

| Cmpd. | λabs [nm] | ε [M-1 cm-1] | λem [nm (eV)] | SS [nm (eV)] | Φf | E0-0 [eV] |
| --- | --- | --- | --- | --- | --- | --- |
| BBT2 | 409 | 33700 | 463 (0.13)a | 54 (0.35) | 18% | 2.78 |
| BBT3 | 420 | 7800 | 491 (0.16)a | 71 (0.43) | 18% | 2.67 |
| BBT4 | 456 | 18600 | 527 | 71 (0.37) | 73% | 2.45 |

[a] In parenthesis the interval between the two vibronic peaks in the emission spectra (in eV).

The experimental absorption maxima for BBT2-4 (Figure 4a) are in good agreement with the computed values (see Table 1), with differences of ca. 0.1 eV. Moreover, the computational analysis reproduced the red-shift of the lowest energy transition going from BBT2 to BBT4. By changing the concentration, the ratio between the absorbance value taken at two different wavelengths (BBT2: 409 nm and 390 nm; BBT3: 400 nm and 420 nm; BBT4: 456 nm and 400 nm) remained constant for all tested molecules, showing that aggregation phenomena in solution were negligible (Figure S3).

Figure 4. (a) BBT2, BBT3 and BBT4 absorbance in toluene (0.01 mM); (b) BBT2, BBT3 and BBT4 emission in toluene (0.01 mM) respectively at 409, 420 and 456 nm excitation wavelength.

All molecules had intense emissions between 400-650 nm. Computations also estimated the vertical S1  S0 emission energies with a high level of accuracy, with an energy difference of less than 0.1 eV, as well as the Stokes shifts (Table 2). BBT2 and BBT3 had similar emission spectra (Figure 4b), showing a marked vibronic progression on their emission band. The shape of the emission spectrum remained unchanged regardless of the concentration, ruling out any aggregation effect for concentrations up to 0.01 mM (Figure S4). The presence of the vibronic structure indicates the occurrence of an important structural rearrangement upon excitation[49]. Unfortunately, this phenomenon led to a decrease in the fluorescence quantum yield (Φf), which was therefore relatively low for BBT2 and BBT3 (Φf = 0.18). However, both molecules displayed a large Stokes shift (Table 3), thus meaning a poor overlap between the absorption and emission spectra and a modest self-absorption, that is a very important feature for the possible use in LSC[20].

In case of BBT4 the vibronic structure of the fluorescence band, peaked at 527 nm in toluene, is less evident, and only a weak shoulder at lower energy is visible. Remarkably, a large Stokes shift of 71 nm (0.37 eV) was found. The fluorescence quantum yield was 0.73, therefore much higher than BBT2 and BBT3. This increase in fluorescence quantum yield might be due to a greater conjugation between the donor and acceptor groups and to a decreased rotational freedom of their connecting bond, resulting in a smaller structural rearrangement of the excited molecule. The reduced vibrational structure of the emission band confirmed this hypothesis.

## Spectroscopic characterisation in polymeric films

Given the promising spectroscopic properties of BBT2-4 compounds in solution, in particular Stokes shifts and Φf, the behaviour of the new molecules was also investigated within polymer matrices. Experiments were performed in poly(methyl methacrylate) (PMMA), which is the most used polymer matrix for LSC devices. The fluorophores were dispersed in PMMA at different concentrations (from 0.2 to 1.8% by weight) obtaining films with a 25 µm ± 5 thickness. The films were light yellow for BBT2, yellow-green for BBT3 or orange-yellow for BBT4 (Figure S6). They are transparent and homogeneous for samples containing BBT3 and BBT4 in all the investigated range of concentration (Figure 5).

Figure 5. PMMA film doped with BBT2-4 at different concentration under the illumination of a Dark Reader Transilluminator at 450 nm

Conversely, BBT2 appeared incompatible with PMMA at concentrations higher than 1.4 wt% with phase separation clearly visible at the macroscopic level (Figure 5) and confirmed by optical microscope analysis (Figure 6). Notably, PMMA films doped with BBT2 displayed the formation of microscopic fluorophore aggregates, appearing mostly phase-separated from the PMMA matrix. Instead, BBT3 and BBT4 resulted quite compatible with PMMA also at the highest fluorophore content of 1.8 wt%, with no clear evidence of microscale phase separation.

Figure 6. Optical microscopy images of PMMA film doped with BBT2, BBT3 and BBT4 at the concentration of 1.8 wt% under the illumination with a long-range UV lamp at 366 nm.

The absorbance of BBT2 / PMMA linearly increased with the concentration for values up to 1.0 wt%. Beyond this concentration value, a drastic reduction in absorption occurred due to the formation of aggregates and phase separation. Other experimental data demonstrated the formation of BBT2 aggregates in the polymer phase, that is (i) the progressive red-shift of both the absorption and emission maxima (figure 7) with modification of the spectra in films at 1.4 wt% and 1.8 wt% contents and (ii) the decrease of the Φf with BBT2 concentration, a phenomenon associated with the ACQ (Aggregation-Caused Quenching) behaviour of the fluorophore[51].

Figure 7. (a) UV-Vis absorption spectra of BBT2/PMMA films as a function of fluorophore concentration (wt%);(b) fluorescence spectra of the same BBT2/PMMA films with an excitation wavelength of 409 nm (Φf is reported in parentheses); (c) UV-Vis absorption spectra of BBT3/PMMA films as a function of fluorophore concentration (wt%); (d) fluorescence spectra of the same BBT3/PMMA films with an excitation wavelength of 424 nm (Φf is reported in parentheses); (e) UV-Vis absorption spectra of BBT3/PMMA films as a function of fluorophore concentration (wt.%); (f) fluorescence spectra of the same BBT4/PMMA films with an excitation wavelength of 456 nm (Φf is reported in parentheses).

BBT3 and BBT4 showed better compatibility with PMMA and the absorbance intensity of the derived films regularly increased with fluorophores concentration, keeping the maximum position almost unchanged (Figure 7). For all molecules, the vibronic structure is no longer visible in the emission spectrum in PMMA, whose maximum overlaps with the lowest energy vibronic peak of the emission spectrum in solution. This can be attributed to the limited rotational freedom experienced by the fluorophores within the solid matrix and to the higher polarity of the latter compared to toluene, favouring less planar conformations with greater charge separation character,[51–53] thus provoking larger Stokes shift in comparison to the toluene solution.

For all molecules, the fluorescence quantum yield decreased with increasing concentration, due to the rising self-absorption caused by a partial overlap between the absorption and emission spectrum[28,54]. Notably, while Φf values of about 10-15% showed by BBT2 in PMMA were considered too low for practical applications in LSC, for all concentrations BBT3 showed consistently higher values than that recorded in solution, in the range of 29-33%, due to the above-mentioned confinement effect.

Two alternative polymeric matrices, poly(cyclohexyl methacrylate) (PCMA) and poly(benzyl methacrylate) (PBzMA) were also investigated, to evaluate the effect of the less polar lateral substituent (i.e., benzyl and cyclohexyl, compared to the traditional methyl ester group in PMMA) on the optical features of the derived films. PBzMA and PCMA are 100% amorphous, transparent and commercially available, features that make them suitable for LSC application. BBT2 and BBT3 presented poor compatibility with the new matrices, showing marked segregation of the fluorophore and formation of macroscopic aggregates (Figure S7). On the contrary, BBT4 was well dispersible within the new matrices (Figure 8), even at the highest concentration of 1.8 wt%, thus providing well homogeneous films. For the three concentrations examined (1.0 wt%, 1.4 wt% and 1.8 wt%) in the two new matrices, the maximum absorption wavelength remained constant and similar to PMMA (around 450-460 nm, Figure 9). The emission peak changed its shape as concentration increases, possibly because of the formation of intermolecular interactions among fluorophore molecules.

The broadening of the emission band observed at higher concentrations could be possibly attributed to the formation of small size aggregates that, however, did not adversely affect the phase dispersion into the polymer. Moreover, the Stokes shifts of BBT4 remained high in PBzMA and PCMA films, with values of about 0.50 eV.

Figure 8. Optical microscopy images of BBT4/PBzMA film (left) and BBT4/PCMA film (right) at a concentration of 1.8 wt% under the illumination with a long-range UV lamp at 366 nm

Figure 9. (a) UV-Vis absorption spectra of BBT4/PBzMA films as a function of fluorophore concentration (wt.%); (b) fluorescence spectra of the same BBT4/PBzMA films with an excitation wavelength of 456 nm (Φf values are reported in parentheses); (c) UV-Vis absorption spectra of BBT4/PCMA films as a function of fluorophore concentration (wt.%); (d) fluorescence spectra of the same BBT4/PCMA films with an excitation wavelength of 456 nm (Φf values are reported in parentheses).

The quantum yield rose to 52.6% for BBT4/PBzMA (1.0 wt%) and 65.6% for BBT4/PCMA (1.4 wt%) in comparison with 41.5% previously registered for BBT4/PMMA (1.0 wt%). Such an increase can be attributed to the greater hydrophobicity of PBzMA and PCMA matrices compared to PMMA, possibly inducing a smaller stabilisation of the charge separation state of the excited fluorophore, in turn reducing the weight of non-radiative recombination channels[55].

## Transient absorption spectroscopy

To further characterise the excited states of BBT2-4 chromophores and investigate the dynamics of relaxation after light absorption, femtosecond transient absorption spectra have been recorded both in solution and PMMA matrix. The samples were excited at 400 nm, at the blue edge of absorption of the BBT core, and their transient spectra were recorded in the 0.1 ps-1.5 ns time interval.

The results were analysed by simultaneously fitting all the kinetic traces with a combination of exponential functions (global analysis), and using a kinetic scheme based on a sequential decay. Beside kinetic constants, global analysis also retrieves the correspondent spectral components, indicated as Evolution Associated Difference Spectra (EADS). The transient absorption spectra of BBT2 and BBT4 recorded in toluene are reported in Figure 10a and b, with the correspondent EADS obtained from global analysis (Fig 10c and d)

Figure 10 Transient absorption spectra recorded for a) BBT2 and b) BBT4 in toluene with excitation at 400 nm. Panels c) and d) reports the corresponding Evolution Associated Difference Spectra and lifetimes obtained from Global Analysis of the transient data.

The transient spectra of BBT2 present a negative band peaked at about 500 nm, in the wavelength interval where fluorescence is observed, thus associated to the stimulated emission of the sample, and a broad positive band spanning from about 570 nm to >750 nm, assigned as an excited state absorption (ESA). The transient spectra of BBT4 are qualitatively similar, but being the absorption profile of this sample red shifted in comparison to BBT2, a ground state bleaching band is also visible, peaking at about 500 nm. Analysis of the EADS reported in panels c and d of Figure 10 allows to follow the spectral changes associated to the excited state decay of the samples and the correspondent timescale. The initial spectral component (black line, Figure 11c and d) represents the transient spectrum of the Franck-Condon state, reached immediately after excitation. In <1 ps an evolution is observed, most probably associated to a fast electronic relaxation of the system. In case of BBT2 the relaxation is spectrally manifested with an intensity increase and red shift of the stimulated emission signal, while for BBT4 we observe a partial recovery of the sharp bleaching band and a broadening and red shift of the stimulated emission (evolution from black to red line). On the following timescale (7.6 ps for BBT2, 5.6 ps for BBT4) the stimulated emission band becomes more structured. This is particularly evident for BBT2, where a double peak structure with maxima at about 495 nm and 535 nm appears. This evolution is most probably associated with a structural relaxation occurring in the excited state because of solvent rearrangement and, as suggested from the computed geometrical changes between ground and excited state, mostly involves a planarisation of the molecule due to the rotation of the donor groups. The signal intensity then mostly decays on the following 415 ps timescale for BBT2 (772 ps for BBT4) leaving a small residual component, whose lifetime is longer than the maximum pump-probe delay accessed within our measurement (1.5 ns). It is worth noticing that the evolution of the ESA band in both samples is quite limited, suggesting that the electronic distribution in the excited state does not significantly change in the investigated time interval, and no intermediate dark states are involved in the relaxation of the systems towards the ground state. Excitation at 400 nm thus brings the molecules in their S1 state, which is a charge transfer state because of the D-A-D structure of the samples, and the large Stokes-shift observed (see also the DFT orbitals in Figure S2), from which they decay directly to the ground state.

The comparison of the kinetic traces registered for the two samples on the ESA band, at 665 nm (Figure 11) shows that BBT2 decays faster than BBT4, also presenting a minor residual signal on the long timescale. This result agrees with the lower measured fluorescence quantum yield of BBT2 compared to BBT4.

Figure 11. Comparison between the kinetic traces at 665 nm (ESA band) of BBT2 (closed symbols) and BBT4 (open symbols) in toluene. Continuous lines represent the fit obtained from global analysis.

To complete the excited state characterisation of the samples, transient spectra were also measured for the dyes dispersed in PMMA films. For all samples, the transient spectra recorded in PMMA are qualitatively similar to those recorded in solution. As visible in Figure 12a, reporting the EADS obtained from global analysis of the transient data measured for a 1.0 wt% dispersion of BBT4 in PMMA (spectra and EADS of the other samples are reported in SI), a negative bleaching/stimulated emission signal and a broad ESA band are also observed in this case. The negative band however appears less structured and presents a less extended band shape evolution in time if compared to the solution. This is readily explained through the prevention of vibrational and structural relaxation in the polymer matrix. The comparison of the kinetic traces measured at 665 nm for BBT4 in toluene and PMMA, reported in Figure 12b, shows that the signal recovery is faster in the matrix and that the residual observed on the long timescale has lower intensity. This observation points to an increased radiationless relaxation in PMMA compared to the solution, which agrees with the decreased fluorescence QY measured for a 1.0 wt% dispersion of BBT4 in PMMA compared to toluene. This could be due to the possibility that the geometry adopted by this compound in the matrix is more twisted compared to the solution, stabilising charge separation and lowering the energy gap between the excited and ground state, which in turn would decrease the excited state lifetime and decrease the fluorescence quantum yield.

Figure 12. a) Evolution Associated Difference Spectra obtained from global analysis of the transient absorption data measured for BBT4/PMMA upon excitation at 400 nm; b) Comparison between the kinetic traces at 665 nm (ESA band) of BBT4 in toluene (open symbols) and PMMA film 1 wt% (closed symbols) with fit (red lines).

## Optical efficiencies

The performances of the fluorophore/polymer films as LSC were determined according to the procedure reported in the experimental part. Notably, the power generated by the photovoltaic cell was measured when directly exposed to the lighting of the AM1.5 solar simulator (PSC) and when combined with the LSC (PLSC). The PLSC/PSC ratio is the concentration factor (C), linked to the optical efficiency (ηopt) through the LSC geometric factor (G), which is the ratio between the area exposed to the light source and the collecting area (i.e., 16.6 in our case, see equation 1, Experimental Section). The results obtained with the derived BBTs were compared with those collected from the reference dye Lumogen Red 305 (LR305, Table 4) under the same conditions. Notably, it appears quite evident how the optical efficiency of the different fluorophore/polymer matrix is connected to the respective fluorescence quantum yield (Figure 13). Nevertheless, Φf is not the only parameter that affects optical efficiency. The large Stokes shift showed by BBT2-4 contributed in limiting the losses in efficiency, despite the poor compatibility with the polymeric matrix and the low fluorescence quantum yield. Indeed, BBT2/PMMA showed optical efficiencies of 5-6%, whereas,  notwithstanding its Φf > 90%, LR305 in PMMA did not exceed optical efficiencies of 10%, due to an evident overlap between the absorption and emission spectrum.[56]

Figure 13. (a) Φf values (%) and (b) optical efficiencies (ηopt) of the fluorophores tested in films at different concentration.

The combination of large Stokes shift and Φf values around 30% increased the optical efficiency of PMMA films containing BBT3 and BBT4 fluorophore up to about 6 and 7%, respectively (Figure 13). The observed different performances of these two fluorophores can be possibly ascribed to the evident red-shift of about 50 nm of both the maximum absorption and emission of BBT4 in PMMA (Figure 7). In fact, while approaching the zone of maximum intensity of the solar spectrum in absorption provides better solar harvesting features, shifting the emission towards the best operation window of the silicon-based cell increases the efficiency of the light-current process, that in turn boosts the LSC overall performances. [add ref 23]

Table 4. Best optical efficiency (ηopt) and concentration factor (C) obtained for fluorophore/polymer BBTs series in comparison with LR305.

| Fluorophore | Polymer | Concentration (wt%) | ηopt (%)a | Ca |
| --- | --- | --- | --- | --- |
| BBT2 | PMMA | 1.0 | 5.8 | 0.97 |
| BBT3 | PMMA | 1.0 | 6.5 | 1.08 |
| BBT4 | PMMA | 1.4 | 7.5 | 1.25 |
| BBT4 | PBzMA | 1.0 | 8.5 | 1.42 |
| BBT4 | PCMA | 1.4 | 9.0 | 1.50 |
| LR305 | PMMA | 1.4 | 10.1 | 1.68 |
| LR305 | PCMA | 1.0 | 9.1 | 1.52 |

aηopt and C data were characterized by standard deviations of 0.5 and 0.1, respectively

In the case of BBT4, the use of alternative polymer matrices promoted a considerable increase in fluorescence quantum yield (Figure 9) and greater optical efficiencies were measured both in PBzMA (8.5% at 1 wt% concentration) and in PCMA (9.0% at 1.4% concentration). Remarkably, for these types of fluorophores, the decrease in the polarity of the matrix favored not only a better dispersion of the fluorophore but also increased the relaxation of the excited state through radiative channels. The optimal concentrations of the fluorophore were found to be 1.0 and 1.4 wt%, respectively, while beyond these values no increase in efficiencies was recorded. The values obtained were very close to those measured with the LR305 reference fluorophore that did not apparently benefit from the PCMA matrix in the range of concentration investigated. The importance of the LSC devices based on the BBT3-4 fluorophores resulted even more evident when considering the concentration factor C that for practical applications must be higher than 1. To our knowledge, there are a few examples of small area devices (25 cm2 or less) based on organic emitters that reported C factor greater than 1[57] and only two greater than 1.50 [58,59], i.e. the maximum value gathered in this work for the BTT4/PCMA system.

# Conclusions

In summary, we obtained a series of three new BBT-based fluorescent molecules with a very straightforward synthesis and with good yields that are essential to promote their use in the LSC technology. The absorption wavelength was tuned adequately by changing the donor moiety bound to the BBT acceptor core. All the three molecules showed an intense emission spectrum between 460 and 550 nm, overlapping the light-absorption spectrum of a Si-based photovoltaic cell, and down-converting the blue part of the solar spectrum where the efficiency of Si-cells is usually low. Furthermore, Stokes shifts were large enough to minimise the self-absorption effects of the fluorophores. Computational analysis showed that the major transition involves a charge separation process that causes a planarization of the molecule in the excited state. BBT2 and BBT3 behave very similarly and exhibit a relatively low fluorescence quantum yield, which can be ascribed to non-radiative relaxation phenomena. Φf values up to 73% were recorded for BBT4 in toluene and with an emission depending on the environment polarity. The TAS studies, showed that the excited state absorption of BBT4 decayed more rapidly in PMMA than in toluene, and it was characterised by a lower residual intensity. This phenomenon appeared mitigated by the dispersion in less polar matrices such as PBzMA and PCMA, in agreement with an increase of Φf. The LSC devices built with BBT dyes were characterised by good transparency and different colours ranging from light yellow to orange. BBT2 and BBT3 showed relatively low Φf in PMMA (approx. 16% and 31%, respectively), and optical efficiencies of 5.8% and 6.5%, respectively, that were favourably affected by the large Stokes shift that, in turn, limited the efficiency losses within the waveguide. Notably, BBT4 gave LSCs C factor >1 for all polymeric matrices and with maximum optical efficiencies of 9.0% in the less polar PCMA matrix, in agreement with the computational and TAS investigations. This performance is very similar to the best data obtained by LR305 in PMMA. Nevertheless, the larger Stokes shifts and the consequent lower self-absorption than LR305 suggest that the BBT-series fluorophores could possibly attain better optical efficiencies in large surface area LSC devices.

ACKNOWLEDGMENTS

We thank “Fondazione Cassa di Risparmio di Firenze” (SUNNYSIDE project, grant no. 2020.1408) for financial support. A. S. and C. C. acknowledge MIUR Grant - Department of Excellence 2018-2022.

# Bibliography

[1]	Lee TD, Ebong AU. A review of thin film solar cell technologies and challenges. Renew Sustain Energy Rev 2017;70:1286–97. https://doi.org/10.1016/j.rser.2016.12.028.

[2]	Le Donne A, Scaccabarozzi A, Tombolato S, Marchionna S, Garattini P, Vodopivec B, et al. State of the Art and Perspectives of Inorganic Photovoltaics. ISRN Renew Energy 2013;2013:1–8. https://doi.org/10.1155/2013/830731.

[3]	Gong J, Sumathy K, Qiao Q, Zhou Z. Review on dye-sensitized solar cells (DSSCs): Advanced techniques and research trends. Renew Sustain Energy Rev 2017;68:234–46. https://doi.org/10.1016/j.rser.2016.09.097.

[4]	Hagfeldt A, Boschloo G, Sun L, Kloo L, Pettersson H. Dye-sensitized solar cells. Chem Rev 2010;110:6595–663. https://doi.org/10.1021/cr900356p.

[5]	Roy P, Kumar Sinha N, Tiwari S, Khare A. A review on perovskite solar cells: Evolution of architecture, fabrication techniques, commercialization issues and status. Sol Energy 2020;198:665–88. https://doi.org/10.1016/j.solener.2020.01.080.

[6]	Correa-Baena JP, Abate A, Saliba M, Tress W, Jesper Jacobsson T, Grätzel M, et al. The rapid evolution of highly efficient perovskite solar cells. Energy Environ Sci 2017;10:710–27. https://doi.org/10.1039/c6ee03397k.

[7]	Weber WH, Lambe J. Luminescent greenhouse collector for solar radiation. Appl Opt 1976;15:2299. https://doi.org/10.1364/ao.15.002299.

[8]	Batchelder JS, Zewai AH, Cole T. Luminescent solar concentrators 1: Theory of operation and techniques for performance evaluation. Appl Opt 1979;18:3090. https://doi.org/10.1364/AO.18.003090.

[9]	Meinardi F, Colombo A, Velizhanin KA, Simonutti R, Lorenzon M, Beverina L, et al. Large-area luminescent solar concentrators based on ‘Stokes-shift-engineered’ nanocrystals in a mass-polymerized PMMA matrix. Nat Photonics 2014;8:392–9. https://doi.org/10.1038/nphoton.2014.54.

[10]	Coropceanu I, Bawendi MG. Core/shell quantum dot based luminescent solar concentrators with reduced reabsorption and enhanced efficiency. Nano Lett 2014;14:4097–101. https://doi.org/10.1021/nl501627e.

[11]	Meinardi F, Bruni F, Brovelli S. Luminescent solar concentrators for building-integrated photovoltaics. Nat Rev Mater 2017;2:17072. https://doi.org/10.1038/natrevmats.2017.72.

[12]	Bünzli J-CG, Chauvin A-S. Lanthanides in Solar Energy Conversion. Handb. Phys. Chem. Rare Earths, 2014, p. 169–281. https://doi.org/10.1016/B978-0-444-62711-7.00261-9.

[13]	McKenna B, Evans RC. Towards Efficient Spectral Converters through Materials Design for Luminescent Solar Devices. Adv Mater 2017;29:1606491. https://doi.org/10.1002/adma.201606491.

[14]	Davis NJLK, Macqueen RW, Jones STE, Orofino-Pena C, Cortizo-Lacalle D, Taylor RGD, et al. Star-shaped fluorene-BODIPY oligomers: versatile donor-acceptor systems for luminescent solar concentrators † ‡. J Mater Chem C 1952;5:1952. https://doi.org/10.1039/c6tc05298c.

[15]	Lee WWH, Zhao Z, Cai Y, Xu Z, Yu Y, Xiong Y, et al. Facile access to deep red/near-infrared emissive AIEgens for efficient non-doped OLEDs. Chem Sci 2018;9:6118–25. https://doi.org/10.1039/c8sc01377b.

[16]	Iagatti A, Patrizi B, Basagni A, Marcelli A, Alessi A, Zanardi S, et al. Cite this. Phys Chem Chem Phys 2017;19:13604. https://doi.org/10.1039/c6cp08721c.

[17]	Patrizi B, Iagatti A, Abbondanza L, Bussotti L, Zanardi S, Salvalaggio M, et al. Ultrafast Intramolecular and Solvation Dynamics in 4,7-Bis (4,5-dibutylbenzo[1,2-b:4,3-b′]bisthiophene[1,2-b:4,3-b′]bisthiophen-2-yl)-2,1,3-benzothiadiazole 2019. https://doi.org/10.1021/acs.jpcc.8b11191.

[18]	Lucarelli J, Lessi M, Manzini C, Minei P, Bellina F, Pucci A. “N-alkyl diketopyrrolopyrrole-based fluorophores for luminescent solar concentrators: Effect of the alkyl chain on dye efficiency.” Dye Pigment 2016;135:154–62. https://doi.org/10.1016/j.dyepig.2016.03.036.

[19]	Papucci C, Geervliet TA, Franchi D, Bettucci O, Mordini A, Reginato G, et al. Green/Yellow-Emitting Conjugated Heterocyclic Fluorophores for Luminescent Solar Concentrators. European J Org Chem 2018;2018:2657–66. https://doi.org/10.1002/ejoc.201800242.

[20]	Sala P Della, Buccheri N, Sanzone A, Sassi M, Neri P, Talotta C, et al. First demonstration of the use of very large Stokes shift cycloparaphenylenes as promising organic luminophores for transparent luminescent solar concentrators †. This J Is Cite This Chem Commun 2019;55:3160. https://doi.org/10.1039/c8cc09859j.

[21]	Still WC, Kahn M, Mitra A. Rapid Chromatographic Technique for Preparative Separations with Moderate Resolution. J Org Chem 1978;43:2923–5. https://doi.org/10.1021/jo00408a041.

[22]	Albano G, Colli T, Nucci L, Charaf R, Biver T, Pucci A, et al. Synthesis of new bis[1-(thiophenyl)propynones] as potential organic dyes for colorless luminescent solar concentrators (LSCs). Dye Pigment 2020;174:108100. https://doi.org/10.1016/j.dyepig.2019.108100.

[23]	Albano G, Colli T, Biver T, Aronica LA, Pucci A. Photophysical properties of new p-phenylene- and benzodithiophene-based fluorophores for luminescent solar concentrators (LSCs). Dye Pigment 2020;178:108368. https://doi.org/10.1016/j.dyepig.2020.108368.

[24]	Geervliet TA, Gavrila I, Iasilli G, Picchioni F, Pucci A. Luminescent Solar Concentrators Based on Renewable Polyester Matrices. Chem – An Asian J 2019;14:877–83. https://doi.org/10.1002/asia.201801690.

[25]	Mori R, Iasilli G, Lessi M, Belén Muñoz-García A, Pavone M, Bellina F, et al. Polymer Chemistry rsc.li/polymers Luminescent solar concentrators based on PMMA films obtained from a red-emitting ATRP initiator †. Polym Chem 2018;9:1168. https://doi.org/10.1039/c7py01933e.

[26]	Sottile M, Tomei G, Borsacchi S, Martini F, Geppi M, Ruggeri G, et al. Epoxy resin doped with Coumarin 6: Example of accessible luminescent collectors. Eur Polym J 2017;89:23–33. https://doi.org/10.1016/j.eurpolymj.2017.02.003.

[27]	Gianfaldoni F, De Nisi F, Iasilli G, Panniello A, Fanizza E, Striccoli M, et al. A push-pull silafluorene fluorophore for highly efficient luminescent solar concentrators. RSC Adv 2017;7:37302–9. https://doi.org/10.1039/c7ra08022k.

[28]	Lucarelli J, Lessi M, Manzini C, Minei P, Bellina F, Pucci A. ``N-alkyl diketopyrrolopyrrole-based fluorophores for luminescent solar concentrators: Effect of the alkyl chain on dye efficiency’’. Dye Pigment 2016;135:154–62. https://doi.org/10.1016/j.dyepig.2016.03.036.

[29]	Pina J, Sarmento D, Accoto M, Gentili PL, Vaccaro L, Adelino G, et al. No Title. J Phys Chem B 2017;121:2308–18.

[30]	Di Donato M, Iagatti A, Lapini A, Foggi P, Cicchi S, Lascialfari L, et al. Combined experimental and theoretical study of efficient and ultrafast energy transfer in a molecular dyad. J Phys Chem C 2014;118:23476–86. https://doi.org/10.1021/jp505957q.

[31]	Henry ER. The Use of Matrix Methods in the Modeling of Spectroscopic Data Sets. Biophys J 1997;72:652–73.

[32]	Van Stokkum IHM, Larsen DS, Van Grondelle R. Global and target analysis of time-resolved spectra. Biochim Biophys Acta - Bioenerg 2004;1657:82–104. https://doi.org/10.1016/j.bbabio.2004.04.011.

[33]	Snellenburg JJ, Laptenok S, Seger R, Mullen KM, van Stokkum IHM. Glotaran: A Java-based graphical user interface for the R package TIMP. J Stat Softw 2012;49:1–22. https://doi.org/10.18637/jss.v049.i03.

[34]	Hohenberg P, Kohn W. Inhomogeneous Electron Gas. Phys Rev 1964;136:864–71.

[35]	Kohn W, Sham LJ. Self-Consistent Equations Including Exchange and Correlation Effects. Phys Rev 1965;140:A1133–8. https://doi.org/10.1103/PhysRev.140.A1133.

[36]	Parr RG, Yang W. Density‐functional theory of atoms and molecules. Oxford Uni. New York, Oxford: 1989.

[37]	Adamo C, Jacquemin D. The calculations of excited-state properties with time-dependent density functional theory. Chem Soc Rev 2013;42:845–56. https://doi.org/10.1039/c2cs35394f.

[38]	Laurent AD, Adamo C, Jacquemin D. Dye chemistry with time-dependent density functional theory. Phys. Chem. Chem. Phys., vol. 16, Royal Society of Chemistry; 2014, p. 14334–56. https://doi.org/10.1039/c3cp55336a.

[39]	Firsch MJ, Trucks GW, Schlegel HB, Scuseria GE, Robb MA, Cheeseman JR, et al. Gaussian 09, Revision C.01 2010.

[40]	Becke AD. Density‐functional thermochemistry. III. The role of exact exchange. J Chem Phys 1993;98:5648–52. https://doi.org/10.1063/1.464913.

[41]	Lee C, Yang W, Parr RG. Development of the Colle-Salvetti correlation-energy formula into a functional of the electron density. Phys Rev B 1988;37:785–9. https://doi.org/10.1103/PhysRevB.37.785.

[42]	Yanai T, Tew DP, Handy NC. A new hybrid exchange–correlation functional using the Coulomb-attenuating method (CAM-B3LYP). Chem Phys Lett 2004;393:51–7. https://doi.org/10.1016/j.cplett.2004.06.011.

[43]	Lynch BJ, Fast PL, Harris M, Truhlar DG. Adiabatic Connection for Kinetics. J Phys Chem A 2000;104:4811–5. https://doi.org/10.1021/jp000497z.

[44]	Tomasi J, Mennucci B, Cammi R. Quantum Mechanical Continuum Solvation Models. Chem Rev 2005;105:2999–3094. https://doi.org/10.1021/cr9904009.

[45]	Lucarelli J, Lessi M, Manzini C, Minei P, Bellina F, Pucci A. ``N-alkyl diketopyrrolopyrrole-based fluorophores for luminescent solar concentrators: Effect of the alkyl chain on dye efficiency’’. Dye Pigment 2016;135:154–62. https://doi.org/10.1016/j.dyepig.2016.03.036.

[46]	Iasilli G, Francischello R, Lova P, Silvano S, Surace A, Pesce G, et al. Luminescent solar concentrators: boosted optical efficiency by polymer dielectric mirrors †. Mater Chem Front 2019;3:429. https://doi.org/10.1039/c8qm00595h.

[47]	De Nisi F, Francischello R, Battisti A, Panniello A, Fanizza E, Striccoli M, et al. Red-emitting AIEgen for luminescent solar concentrators †. Chem Front 2017;1:1406. https://doi.org/10.1039/c7qm00008a.

[48]	Carlotti M, Fanizza E, Panniello A, Pucci A. A fast and effective procedure for the optical efficiency determination of luminescent solar concentrators. Sol Energy 2015;119:452–60. https://doi.org/10.1016/j.solener.2015.05.031.

[49]	Omary MA, Patterson HH. Luminescence, Theory. Encycl. Spectrosc. Spectrom., Elsevier Inc.; 2017, p. 636–53. https://doi.org/10.1016/B978-0-12-803224-4.00193-X.

[50]	Zhou W, Zhao B, Shen P, Jiang S, Huang H, Deng L, et al. Multi-alkylthienyl appended porphyrins for efficient dye-sensitized solar cells. Dye Pigment 2011;91:404–12. https://doi.org/10.1016/j.dyepig.2011.05.017.

[51]	Mei J, Hong Y, Lam JWY, Qin A, Tang Y, Tang BZ. Aggregation-induced emission: The whole is more brilliant than the parts. Adv Mater 2014;26:5429–79. https://doi.org/10.1002/adma.201401356.

[52]	Sasaki S, Drummen GPC, Konishi GI. Recent advances in twisted intramolecular charge transfer (TICT) fluorescence and related phenomena in materials chemistry. J Mater Chem C 2016;4:2731–43. https://doi.org/10.1039/c5tc03933a.

[53]	Valeur B, Berberan-Santos MN. Molecular Fluorescence. Weinheim, Germany: Wiley-VCH Verlag GmbH & Co. KGaA; 2012. https://doi.org/10.1002/9783527650002.

[54]	Donati F, Pucci A, Cappelli C, Mennucci B, Ruggeri G. Modulation of the Optical Response of Polyethylene Films Containing Luminescent Perylene Chromophores. J Phys Chem B 2008;112:3668–79. https://doi.org/10.1021/jp711193u.

[55]	Clarke TM, Gordon KC, Kwok WM, Phillips DL, Officer DL. Tuning from π,π* to Charge-Transfer Excited States in Styryl-Substituted Terthiophenes: An Ultrafast and Steady-State Emission Study. J Phys Chem A 2006;110:7696–702. https://doi.org/10.1021/jp0600312.

[56]	Green AP, Buckley AR. Solid state concentration quenching of organic fluorophores in PMMA †. Phys Chem Chem Phys 2015;17:1435. https://doi.org/10.1039/c4cp05244g.

[57]	Roncali J. Luminescent Solar Collectors: Quo Vadis? Adv Energy Mater 2020;10:2001907. https://doi.org/10.1002/aenm.202001907.

[58]	Bomm J, Büchtemann A, Chatten AJ, Bose R, Farrell DJ, Chan NLA, et al. Fabrication and full characterization of state-of-the-art quantum dot luminescent solar concentrators. Sol Energy Mater Sol Cells 2011;95:2087–94. https://doi.org/10.1016/j.solmat.2011.02.027.

[59]	Mateen F, Ali M, Lee SY, Jeong SH, Ko MJ, Hong SK. Tandem structured luminescent solar concentrator based on inorganic carbon quantum dots and organic dyes. Sol Energy 2019;190:488–94. https://doi.org/10.1016/j.solener.2019.08.045.