Depolymerization of polyethylene terephthalate (PET) under mild conditions by Lewis/Brønsted acidic deep eutectic solvents

Marco Rollo,a Francesca Raffi,a Elisa Rossi,a Matteo Tiecco,b Elisa Martinelli,a Gianluca Ciancaleonia

a Department of Chemistry and Industrial Chemistry, University of Pisa, via Giuseppe Moruzzi 13, I-56124 Pisa, Italy

b Chemistry Interdisciplinary Project (ChIP), School of Pharmacy, University of Camerino, via Madonna delle Carceri, 62032 Camerino (MC), Italy

Abstract

Modern society urgently needs new recycling methods to handle the impressive amount of plastic items that are annually discarded. Deep Eutectic Solvents (DESs) have shown interesting results in the depolymerization of polyethylene terephthalate (PET), but most of the procedures still need harsh conditions of temperature and pressure. In this contribution, we propose a bifunctional Lewis/Brønsted acidic DES composed of FeCl3∙6H2O, cheap and scarcely toxic, in combination with a variety of acids, both mineral and organic, including some of natural origin (citric and acetic acid). We show that the LBDES formed with methanesulfonic acid and para-toluenesulfonic acid are capable of quantitatively depolymerizing PET under mild conditions, with a temperature of 100 °C and a reaction time of 1 h, affording high purity terephthalic acid in high yield. For acetic acid, a reaction time of 3 h are necessary to obtain a quantitative depolymerization. Different strategies to optimize the PET/LBDES ratio has been successfully tested, as the consecutive addition of multiple aliquots of PET or the filtration and reuse of the solvent.

The best solvent has been characterized through the comparison of theoretical and experimental eutectic phase diagram, confirming its nature of DES.

Introduction

Polyethylene terephthalate (PET) is a thermoplastic polymer used for its great versatility. Excellent barrier proprieties against oxygen, carbon dioxide and moisture, light weight, high durability, excellent resistance to wear, excellent thermal stability, good chemical resistance, and high tensile strength have been provided for its development in a huge variety of fields.[1] The global PET market size is expected to grow from $35.47 billion in 2021 to $57.19 billion in 2026 at a compound annual growth rate (CAGR) of 9.9%.[2]

“Reduce, reuse, and recycle” should always be the priorities in waste management, but as a matter of fact the PET production is increasing and only a fraction of the PET items is recycled, the rest going to landfill or incineration.

Nowadays, most of the recycling procedures are mechanic, which imply items cleaning, shredding into pellets and reprocessing. These methods are limited by cost, degradation of mechanical properties, and general production of downgrading materials. Some of these drawbacks could be avoided by using chemical recycling methods, as complementary to traditional recycling processes, especially when they selectively return the polymer to its monomeric feedstocks (Scheme 1).[3–5]

Scheme 1. General reactions involved in the chemical recycling of PET.

Such methods can be divided by the conditions used (acidic,[6] basic[7] or neutral[8]) or by the employed nucleophile (glyco-,[9] hydro-,[10] methano-[11] and aminolysis[12]). Generally, all these methods require harsh conditions of temperature (often higher than 180 °C) and pressure (1-5 MPa). In the last years, many studies focused on the use of new solvents to depolymerize PET, as ionic liquids (ILs, which are salts with a melting point lower than 100 °C[13],[14–17]) and deep eutectic solvents (DESs, which are mixtures of two or three chemical compounds with a resulting melting point much lower than those of isolated components[18],[19–22]). DESs, in particular, are interesting because of their structural and functional versatility, their ease of preparation and purification and their potential scalability.[23] When natural compounds are used (aminoacids, simple carbohydrates, molecules involved in biological cycles…) they can be called NADES[24] and they are biodegradable solvents[25]. Alternatively, they can be prepared using  acids[26] or bases,[27,28] allowing a wide tunability of their properties.

In 2015, Wang et al., reported for the first time a fast and selective glycolysis of PET into bis(2-hydroxyethyl) terephthalate (BHET), using urea/ZnCl2 DES. In this reaction, the cooperation of the H-bonds and coordination bonds between the DES and ethylene glycol (EG) supposedly plays an essential role in the high efficiency of the reaction.[19] More recently, Attallah et al., announced the first application of DESs on PET hydrolysis via microwave-assisted process. The aromatic nature of one component of the DES (constituted by m-cresol and choline chloride) is thought to be crucial in the solubilization of PET, due to a strong π…π interaction with the PET, facilitating the contact with the depolymerization agent (NaOH) under microwave irradiation: in 90 s, it was achieved 91.55% terephthalic acid monomer yield from post-consumer bottle.[21]

As both Lewis[10] and Brønsted[29] acids have been tested as catalysts for PET depolymerization, it was interesting to test a solvent made of both of them, with the aim to maximize their concentration and, hopefully, their synergy. Some bifunctional Lewis/Brønsted acidic DESs (LBDESs) have been recently prepared and applied in the desulfurization of diesel fuels[30] and bio-mass treatment,[31–33] but, to the best of our knowledge, no report about their application in PET depolymerization is available to date. In one case, a zeolite with Lewis and Brønsted acidic sites has been used (reaction temperature between 130 and 230 °C, reaction time between 10 and 40 min),[34] showing that their synergy is important to enhance the depolymerization yield.

In this paper, FeCl3∙6H2O has been chosen as Lewis acid, because of the low price and scarce toxicity of iron. On the other hand, many Brønsted acids have been tested, varying their strength, hydrophilicity, and biocompatibility. In particular, the novel combinations iron chloride/sulfonic acids showed great performance and has been thoroughly characterized, showing to be a real DES and not a simple solution or a eutectic mixture of the components. About PET depolymerization, the effects of process parameters, including time, temperature, progressive addition of PET’s flakes, and water content were examined. The maximum conversion of PET and yield of terephthalic acid were found to be 100% and 98% respectively, after one hour at 100 °C and atmospheric pressure by using FeCl3∙6H2O/methanesulfonic acid (MSA) 1:1 (system A1_1) molar ratio as DES. Analytical methods, including Fourier transform-infrared spectroscopy (FT-IR), nuclear magnetic resonance (NMR), gas chromatography (GC) and elemental analysis were successfully employed to check the quality of the terephthalic acid obtained from post-consumer PET bottles, which resulted to have a purity higher than 98%.

Results and Discussion

PET depolymerization. In order to prepare mixed Lewis/Brønsted acidic mixtures, iron(III) chloride hexahydrate (FeCl3∙6H2O) was mixed and heated in different molar ratios (generally spanning from FeCl3∙6H2O/acid 3:1 to 1:2) with different organic acids and substances (see Experimental Section). Table 1 shows the results of this extensive screening, highlighting the combinations that lead to homogeneous liquids. In some cases, the liquid is kinetically unstable and turns into a heterogeneous system within some hours (>12 h in the case of FeCl3∙6H2O/p-toluenesulfonic acid (pTSA) 1:1 molar ratio, system B1_1). While some of the presented mixtures are already known (as FeCl3∙6H2O/glycine and FeCl3∙6H2O/malonic acid[26,33]), the liquids formed with sulfonic acids are, to the best of our knowledge, novel and particularly interesting because of their strong acidity.

Table 1. Screening of the liquid formation with FeCl3∙6H2O: hom = homogeneous, het = heterogeneous, un = unstable, - = not tested. The different stoichiometry ratios refer to FeCl3∙6H2O: substance.

| Substance | 3:1 | 2:1 | 1:1 | 1:2 |
| --- | --- | --- | --- | --- |
| MSA | hom | hom | hom | hom |
| pTSA∙H2O | het | hom/un | hom/un | hom/un |
| p-phenol-sulfonic acidd | - | - | hom | - |
| sulfuric acid | homa | hetb | hetc | - |
| acetic acid | - | - | hom | - |
| citric acid | hom | hom | hom | - |
| tartaric acid | - | het | het | - |
| malonic acid | - | - | hom/un | - |
| levulinic acid | - | - | hom | - |
| myristic acid | - | - | het | - |
| succinic acid | - | - | het | - |
| propanoic acid | - | - | hom/un | - |
| hexanoic acid | - | het | het | het |
| nonanoic acid | - | - | het | - |
| gallic acid | - | - | het | - |
| oxalic acid | - | hom | hom/un | - |
| ascorbic acid | - | het | het | - |
| 4-hydroxy-benzoic acid | - | het | het | - |
| benzoic acid | - | het | het | - |
| phenyl-acetic acid | - | hom/un | hom/un | - |
| phenyl-propanoic acid | - | - | hom/un | - |
| glycolic acid | - | - | hom | - |
| malic acid | - | hom | hom/un | - |
| glycine | hom | hom | het | - |
| L-arginine | - | het | het | - |
| thymol | - | het | het | - |
| pentaerythritol | het | het | het | - |
| D-mannitol | - | hom | het | - |
| glycerol | hom | hom | hom | hom |
| m-cresol | - | - | het | - |
| choline chloride | - | het | het | - |

a With 6 equivalents of water; b with 3 equivalents of water; c with 2 equivalents of water; d in aqueous solution (65%).

In order to test the performance of the various Lewis/Brønsted mixtures in PET depolymerization, we placed 0.3 g of PET flakes (derived from post-consumer colorless water bottle) in 4.0 g of system B1_1 at atmospheric pressure and at the temperature of 130 °C. We performed the reaction in a round-bottom balloon equipped with a condenser to avoid water loss or, with the same results, in a simple glass vial with screw cap. The use of a closed vial was possible because of the low volatility of the DES, which does not evaporate significantly in the range 80-130 °C and the inner pressure does not increase very much.

To our delight, after 1 h all the flakes reacted, leaving a powdery precipitate (see Supporting Information). The heterogeneous mixture was diluted with about 10 mL of deionized water, obtaining a powder that, after purification, was proved to be pure terephthalic acid (TA) by IR, elemental analysis and NMR (see Supporting Information). Importantly, the Inductively Coupled Plasma (ICP) analysis evidenced that the iron content is below 0.3 ppm and comparable to the ubiquitous impurities of other heavy metals (Supporting Information), indicating that all the iron present in the solvent can be washed away without leaving any significant residue in the TA.

The depolymerization efficacy of system B1_1 was investigated and optimized in detail. Firstly, the effect of the temperature was studied, choosing 30 minutes as reaction time (Figure 1). The reaction already proceeded at 80 °C, with a PET conversion of 83.8% and a yield of purified TA of 40.1%. Differently than before, in this case a complex mixture of solids was present at the end of the reaction: unreacted PET flakes, mechanically separated from the rest, TA (which is soluble in basic water) and a third white powder insoluble in both acidic and basic water. This white powder has been analyzed by IR and GPC and resulted to be PET oligomers, with a molecular weight of 1 kDa, whereas the original PET showed a molecular weight around 26 kDa (Supporting Information). Partial depolymerization explained the difference between conversion and yield: PET is initially degraded by random hydrolysis of the ester groups along the polymer backbone, which results into the formation of oligomers with lower molecular weights. As the reaction proceeds further, the molecular weight of oligomers decreases and the formation of the monomers becomes more probable. Conversion rapidly increases to 100% at 90 °C, whereas the yield after 30 minutes reached 83.6% at 120 °C (Figure 1A).

Successively, depolymerization was carried out at 100 °C by changing the reaction time (Figure 1B). Under the same experimental conditions (0.3 g of PET in 4 g of system B1_1), the yield became 88.6% after 1 h, reaching a plateau at longer reaction times. As the conversion was quantitative, the remaining 11.4% is likely lost during the work-up procedure (see Experimental Section) or persisted under the form of oligomers.

The reaction was also carried out by using a pTSA∙H2O/H2O 1:3 mixture, not containing FeCl3∙6H2O, and a FeCl3∙6H2O/H2O 1:1 solution, not containing pTSA, to confirm that the synergistic effect of pTSA and FeCl3 is necessary to depolymerize PET. Indeed, PET conversion was found to be null for the former and negligible (3.2%) for the latter and most of PET flakes were recovered at the end of the reaction.

Figure 1. Screening of the reaction conditions on PET conversion and TA yield. Panel A) reaction temperature (0.3 g of PET, 4.0 g of system B1_1, reaction time = 30 min); panel B) reaction time (0.3 g of PET, 4.0 g of system B1_1, T = 100 °C).

Successively, all the iron-based liquids reported in Table 1 were tested under the same experimental conditions (Figure 2). Many systems showed a certain ability to depolymerize the PET flakes, and stronger Brønsted acids have better conversion and yields. System containing non acidic components (as glycerol, D-mannitol and glycine) showed no conversion, indicating that iron(III) chloride is not enough to carry on the depolymerization reaction. Particularly interesting are the performances of DESs composed by natural acids (as acetic and citric acids) or acids potentially obtained by biomasses and glucose, as malonic[35] and glycolic acids[36], for their biodegradability and renewable origin. The system FeCl3∙6H2O/acetic acid showed 100% conversion and 99.7% yield after 3h at 120 °C, allowing to choose the best mixture that balances all the different aspects (cost/sustainability/toxicology of the acid, corrosion power of the mixture, reaction time and temperature). Anyway, only system A1_1 had superior performance than system B1_1, in terms of both PET conversion and yield of isolated TA. The real eutectic composition (FeCl3∙6H2O/MSA 1:5 molar ratio, system A1_5 see later) showed poorer performance than the 1:1 mixture A1_1, likely for a non-optimal ratio between Lewis and Brønsted acidic sites.

Figure 2. Reaction performance of different Lewis/Brønsted mixtures under the optimized reaction conditions (0.3 g of PET, 4.0 g of LBDES, T = 100 °C, reaction time = 30 min).

Interestingly, a strong mineral acid as H2SO4 showed worse performance than systems A1_1 and B1_1 (conversion 72.3% and yield 61.5%) under our experimental conditions. Sulfuric acid solutions can be used, but longer reaction times and higher temperatures are generally required (yield 80% in four days at 100 °C).[37]

Conversion and yield were also very low (18.9% and 6.2%, respectively) when PET depolymerization was carried out under basic hydrolysis conditions by using a concentrated solution of NaOH (30% w/w) for 30 min at 100 °C. This is consistent with what reported in literature where higher temperatures are generally used to effectively carry out basic hydrolysis of PET,[3] if special additives are not used.[38]

All the previous experiments concur in proving that the synergy between Lewis and Brønsted species is pivotal for the effective depolymerization of PET under the mild conditions of this work. This synergy likely involves a simultaneous “double activation” of the ester groups by the two different acids, but more mechanistic study will be necessary to support this hypothesis. Anyway, the formation of a DES seems to be critical: we tried to mix CoCl2∙6H2O, NiCl2∙6H2O, CuCl2∙2H2O and ZnCl2 with MSA in different molar ratios, but in all the cases, heterogeneous mixtures have been obtained.

A critical point is the dilution effect: indeed, adding other 10 equivalents of water to the systems A1_1 and B1_1, both conversion and yield sensibly decreased from 100% and 96.4% to 23.8% and 15.5% (system A1_1) and from 100% and 88.6% to 6.2% and 1.8% (system B1_1), respectively. By waiting 5 h the performance of diluted A1_1 increased to 46.9% and 36.5%. Intuitively, a three-body adduct as those formed by iron, the ester and the acid proton is favored only at very high concentrations, justifying the use of a DES.

Different sources of post-consumer PET samples have been tested, and for each one the properties of the starting material have been determined (Supporting Information). No appreciable difference has been noted using colorless or colored items, as well as samples from water/milk/carbonated drink bottles or from 100% polyester textile.

In the optimized reaction conditions (0.3 g of PET in 4.0 g of system A1_1), the stoichiometric ratio between the acid and the ester groups of the polymer is around 3.5. In order to increase the amount of PET depolymerized by our solvents, we tried different strategies (Table 2): loading of a larger amount of PET is possible, but some flakes are not covered by the solvent and tend to adhere to the reactor walls, hampering the necessary PET/liquid contact. For example, by loading 4 g of PET in 4 g of system A1_1, at 100 °C for 5 h, the conversion and yield were 47.9% and 48.3%, respectively. Also in this case the necessary PET/DES contact was not guaranteed (Supporting Information). Alternatively, we tried to add a larger amount of PET by different aliquots of 0.3 g per hour of reaction, leaving the workup at the end of the reaction. After each addition, also 56 μL of deionized water were added, with the aim to reintroduce in the solvent the water lost in the hydrolysis. This strategy allowed to depolymerize 1.2 g of PET with 4 g of A1_1 (final conversion 96.2%, yield 97.8%, stoichiometric ratio between the acid and the ester groups of the polymer around 0.9).

Table 2. Optimization of the PET/DES ratio

| Solvent | PET sample | PET/DES (w/w, in g) | reaction time (h) | Conversion (%) | Yield (%) |
| --- | --- | --- | --- | --- | --- |
| system B1_1 | flakes | 0.3/4.0 | 0.5 | 100 | 56.1 |
| system B1_1 | powder | 0.3/4.0 | 0.5 | 92 | 52.9 |
| system A1_1 | flakes | 0.3/4.0 | 0.5 | 100 | 63.0 |
| system A1_1 | flakes | 0.3/4.0 | 1 | 100 | 96.4 |
| system A1_1a | flakes | 0.3/4.0 | 1 | 100 | 96.3 |
| system A1_1 | flakes | 4.0/4.0b | 5 | 48 | 48 |
| system A1_1 | flakes | 1.2/4.0c | 4 | 96.2 | 97.8 |
| system A1_1 | flakes | 1.5/4.0c | 5 | 91.4 | 88.0 |

a solvent filtered after the first cycle and reused directly; b flakes added in one aliquot (see Figure S30, Supporting Information); c flakes added in aliquots of 0.3 g per hour of reaction.

The fifth addition showed lower performance, even if still acceptable (final conversion 91.4%, yield 88.0%). In our opinion, the loss of performance is not due to a dilution effect by the produced EG, as the quantitative depolymerization of 1.2 g of PET means that only 0.39 g of EG are liberated and 0.22 g of water (out of 1.18 g contained in 4.0 g of system A1_1) are consumed by the reaction. Most likely, the solid TA accumulated in the reaction mixture (1.04 g) hampers the PET/DES contact and makes the stirring difficult.

Importantly, the EG that accumulates in the reaction mixture does not interfere with the reaction, as no BHET can be detected. This is likely due to the limited amount of EG produced and the higher reaction temperature that glycolysis generally requires.[1]

The heterogeneous mixture can be filtered at the end of the reaction and the clear liquid can be used again, without any loss of performance. The only drawback here is that the solid materials (unreacted PET, PET oligomers and TA) remain impregnated of the solvent, making its quantitative recover difficult.

Figure 3. Progressive addition of 0.3 g of PET flakes to 4.0 g of system A1_1 (reaction temperature = 100 °C, reaction time = 1.2 h for each addition). In each case, the work-up has been made after the indicated number of additions.

Finally, the procedure was also successfully scaled up, using 100 g of system A1_1 and 30 g of post-user PET flakes, added in 2 aliquots of 15 g with a total reaction time of 3 hours, with unaltered quantitative conversion and high yield. Considering as possible products TA, ethylene glycol and PET oligomers, the atom economy of this process is nearly optimal, as oligomers are almost absent (< 5%) and desired products can be efficiently recovered by basic dissolution/acidic precipitation (TA) and vacuum distillation of the post-reaction liquid phase (EG, Teb = 197 °C at 1 atm), respectively. Regarding iron, at the end of work-up it may be converted in iron oxide and recovered by a magnetic separation, whereas MSA can be distilled away before EG (Teb = 165 °C at 1 atm).

In order to compare the present method with literature ones, an important comparison method is the Environmental factor (E), simply defined as the mass of waste for mass of product. It should be always coupled with other factors, as the energy economy (ε) and the combination of E and ε, (environmental energy impact, ξ).[1] Table 3 compares these factors for the method presented here and other examples taken from literature and relative only to the depolymerization step of the process, as done in the literature.[1] The values indicate that our procedure is competitive with most of the other existing protocols, especially using the optimized strategy of adding PET in four aliquots of 0.3 g each (entry “System A1_1, four addition”, Table 3 and Supporting Information).

Table 3. Comparison of environmental factors (E, ε and ξ) for different chemolytic depolymerization of PET.[1]

| Conditions | E | ε (°C-1 min-1) | ξ (°C min) | ref |
| --- | --- | --- | --- | --- |
| System A1_1, one addition | 11.7 | 1.61E-4 | 7.27E4 | This work |
| System A1_1, four additions | 2.88 | 4.07E-5 | 7.08E4 | This work |
| H2SO4(aq) | 8.87 | 2.22E-5 | 3.99E5 | [37] |
| HNO3/DMSO/Na2SO4 | 4.68 | 5.19E-5 | 9.01E4 | [39] |
| HNO3/DMSO/Na2SO4/H3PO4 | 6.27 | 4.55E-5 | 1.38E5 | [8] |
| NaOH/TOMABa | 28.48 | 2.78E-5 | 1.03E6 | [40] |
| NaOH/microwave | 1.70 | 4.47E-4 | 3.8E3 | [41] |
| Urea/ZnCl2 DES | 0.407 | 1.63E-4 | 2.5E3 | [19] |
| K2CO3/EG DES | 1.33 | 4.07E-5 | 3.3E4 | [20] |

a TOMAB = trioctyl methyl ammonium bromide

DES characterization. System A gives stable homogeneous red liquids in many stoichiometric ratios, from 6:1 to 1:3. In addition, it is the best solvent for the PET depolymerization, and therefore it deserves an in-depth characterization.

In order to elucidate the nature of system A, an analysis of the melting point at the different stoichiometric ratios was conducted. In particular, all the systems going from FeCl3∙6H2O/MSA 1:6 to 3:1 have been prepared, the corresponding melting points (Tm) have been evaluated and compared with the theoretical trend of melting points of the pure substances, both for MSA and FeCl3∙6H2O (Supporting Information). This approach is necessary in order to determine if the novel liquid mixture is a DES or a simple eutectic liquid.[42] Indeed, the theoretical curves of the melting points are based on the thermodynamic definitions of the melting of a molecule (A), in the absence of any specific interaction with the other component (B). Any deviations from ideality, and the consequent deviation of the activity coefficient from 1, is on the contrary evidence of interaction occurring between A and B. These interactions hamper the formation of a regular crystal lattice, with the consequence of lowering the melting point. Nowadays, the comparison of theoretical and experimental curves is mandatory to define whether a liquid is a DES or not. If experimental curves perfectly match the theoretical ones, the most appropriate definition would be Eutectic Solvent (ES).

In Figure 1, the experimental melting points and the theoretical curves (Panel A), and the activity coefficients (Panel B) of the FeCl3∙6H2O/methanesulfonic acid mixtures are reported.

Figure 4. Panel A: experimental/theoretical solid-liquid phase diagrams for the FeCl3∙6H2O/methanesulfonic acid LBDES; Panel B: activity coefficients of the components in the LBDES. Dashed line indicates an ideal mixture.

The experimental melting points are much different from the theoretical curves (Figure 4, Panel A), in particular they are much lower. A eutectic point is detected at the molar ratio of MSA of 0.83 (1:5 molar ratio, system A1_5). Theoretical curves show an intersection about the same value of the molar fraction of acid, but with a much higher melting point (ΔTm over 65 °C). Also, the activity coefficients γi (Figure 4, Panel B) are very far from 1 at all the investigated molar ratios (see Supporting Information), indicating the strong non-ideality of the mixture. The values of γi are close to zero in all the cases. Therefore, on the basis of the deepening of the melting point, the difference from the theoretical curves and the shifts in the activity coefficients, the mixture can be defined as a deep eutectic solvent.

The ionic conductivity of DES A was also measured, in order to have information on the structural features of the liquid in terms of ionic species present in the mixture. The conductivity at room temperature is 42.1 and 21.4 mS/cm, for systems A1_1 and A1_5 (FeCl3∙6H2O/MSA 1:5 molar ratio), similar to those of concentrated aqueous solutions of MSA (38.3 and 37.4 mS/cm for MSA: H2O 1:1 and 1:5, respectively) and iron chloride (6.26 and 22.1 mS/cm for FeCl3∙6H2O: H2O 1:1 and 1:5, respectively). The values are higher than the ones observed typically in DESs, but very similar to the ones reported for other iron-based Deep Eutectic Solvents.[33] This could be due to the higher presence of ionic species in the DES and to their easy mobility in the liquid, facilitated by the low viscosity (below 100 cP, see Experimental Section).

The thermogram of system A1_1 (Figure 5)[43] shows that water is readily lost even before 100 °C. This induces to think that the six molecules of water are not strongly bound to iron. Rather, they are likely displaced, partially at least, from the coordination sphere of the metal and free to diffuse in the liquid, contributing to lower the viscosity of the system.

Figure 5. Thermogravimetric analysis curve for system A1_1 (10 °C/min).

The system B1_1 gave, after heating, a dark red, homogeneous liquid, but after some days a solid phase began to form, therefore the liquid is not stable. Furthermore, varying the molar composition always led to a heterogeneous system, which is not suitable for our scope. In addition, fresh system B1_1 shows a quite high ionic conductivity (26.7 mS/cm at room temperature), much higher than in the case of benzyl-triethyl-ammonium chloride/pTSA and choline chloride/pTSA mixtures[44,45] and similar to that of system A1_1. A more complete characterization of systems A1_1, A1_5 and B1_1 is available in the Supporting Information (IR spectra and thermograms, Supporting Information).

Conclusions

The synergy between Lewis and Brønsted acids in the depolymerization of post-consumer PET has been tested and reported, allowing to the quantitative recovery of high purity terephthalic acid in 1 h at 100 °C. The trend of melting point and activity coefficient with the molar composition have been characterized for the novel (and best performing) LBDES (FeCl3∙6H2O/MSA), revealing a strong deviation from ideality and confirming the real DES nature of the liquid.

Many other acids can be used in combination with FeCl3∙6H2O, with lower but still acceptable results: for example, using acetic acid the yield is quantitative after 3 h. The suggested mechanism for PET depolymerization is the double activation of the ester group, with the metal that coordinates to the carbonyl moiety and the acid that protonates the ether oxygen, sensibly increasing the carbon electrophilicity. The method resulted robust in the treatment of different PET sources (textile, thicker bottles for carbonated drinks or milk, colourless and coloured… ) under the same experimental conditions and with the same final TA purity.

At the end of the reaction, other PET can be added without any loss of performance (four additions) and when the solid TA saturates the reactor, the solvent can be filtered and reused, with the only addition of water to carry on the hydrolysis.

Finally, the strategy of synergically combining Lewis and Brønsted acids confirmed its feasibility for PET depolymerization, and it will be tested under different experimental conditions (for example using ultrasounds, microwave heating and additives) and with other polymers having similar functional groups.

Experimental details

Materials. PET plastics were collected directly from the department garbage containers, washed thoroughly with distilled water, dried and cut into flakes (approximate size 0.5x0.5 cm). Iron(III) chloride hexahydrate (FeCl3∙6H2O) was purchased from Alfa Aesar. Methanesulfonic acid (MSA), p-toluenesulfonic acid monohydrate (pTSA·H2O), acetic acid, L-arginine, glycine, citric acid·H2O, pentaerythritol, glycerol, levulinic acid, choline chloride, succinic acid, propanoic acid, hexanoic acid, nonanoic acid, gallic acid, sulfuric acid, oxalic acid, ascorbic acid, 4-hydroxy-benzoic acid, benzoic acid, phenyl-acetic acid, phenyl-propanoic acid, m-cresol, malic acid, tartaric acid, thymol, D-mannitol, myristic acid, malonic acid, glycolic acid, p-phenol sulfonic acid (aqueous solution 65%), sulfuric acid (H2SO4), hydrochloric acid (HCl 37%), sodium hydroxide (NaOH) were purchased from Sigma Aldrich. All the chemicals in this study were used without further purification.

Synthesis of Lewis/Brønsted mixtures. Different mixtures were synthetized by mixing FeCl3∙6H2O with different hydrogen bond donors in suitable quantities under mild heating until a homogeneous red dark liquid appeared. Table 1 shows the mixtures tested and prepared.

Solid-liquid phase curves determination. The DES A were characterized in terms of comparison between the theoretical solid-liquid phase diagrams with the experimental melting points at different molar ratios.[42,46] The melting points were measured with a thermometer via immersion of the samples in a Dewar with CO2/acetone mixture. The melting points were taken in triplicate to avoid kinetic effect on the melting of the mixtures.

The solid-liquid theoretical curves were determined by using the equation (1) that represents the solid-liquid equilibrium curve:

lnχi∙γi= ∆mhiR ∙ 1Tm,i -1T+ ΔmCpiR ∙ Tm,iT-lnTm,iT-1				(1)

where χi is the mole fraction of component i, γi is its activity coefficient in the liquid phase, ∆mhi and Tm,i are its melting enthalpy and temperature, respectively, ΔmCpi is its heat capacity change upon melting, R is the ideal gas constant, and T is the absolute temperature of the system. This equation can be simplified by considering the heat capacity change upon the melting of a substance as negligible, therefore equation (2) was used:

lnχi∙γi= ∆mhiR ∙ 1Tm,i -1T								(2)

The theoretical melting temperatures were determined from the theoretical curves by considering the activity coefficients γi = 1. The eutectic points were determined as the minimum in the experimental curves and they were compared to the theoretical ones.

The experimental γi values were determined via equation (3) by using the experimentally observed melting temperatures:

γi= exp∆mhiR 1Tm,i -1Tχi									(3)

General procedures for PET hydrolysis. For the catalytic experiments, a 25 mL flask equipped with a magnetic stirrer and reflux condenser was filled with 300 mg of post-consumer PET and 4.0 g of DES. Hydrolysis reactions were carried out in a temperature range from 80 to 120 °C for 15-90 min. When the reaction was completed, about 10 mL of distilled water was added to the reaction solution to precipitate terephthalic acid (TA), which was then collected by sedimentation after centrifugation. Supernatant (straw yellow color) contains an aqueous solution of used DES and EG from PET depolymerization. Then, TA was re-solubilized with an aqueous solution of NaOH (1M), giving di-sodium terephthalate. Unreacted PET (if any) and PET oligomers, insoluble in alkaline medium, was removed manually and by filtration, respectively. PET conversion was calculated using the following equation (4)

PET conversion %=W1-W2W1∙100						(4)

where W1 is the initial weight of PET flakes and W2 is the weight of unreacted PET.

TA was finally precipitated by adding 2 mL of hydrochloric acid (37%) and then collected by filtering. The obtained white powder of TA was then washed with water several times and dried at 80 °C overnight. TA yield was calculated using the following equation (5)

TA yield= WTPA∙MPETMTPA∙W1∙100							(5)

where WTPA is the weight of TA, MTA is the molecular weight of TA and MPET is the molecular weight of PET monomeric unit.

For all the analyses, our TA samples were compared with samples of commercial TA (Merck, purity > 98%), taken as a reference.

Characterization. 1H and 13C NMR measurements were carried out on a FT-NMR Joel JNM-ECZ500R MHz with HFX probe at room temperature.

The Fourier Transform infrared-attenuated total reflectance (FTIR-ATR) spectra of terephthalic acid were recorded using FT-IR Thermoscientific Nicolet iS50 spectrometer equipped with Smart iTR with single reflection diamond crystal (sampling depth 2.03 μm at 1000 cm-1, incidence angle 42°). The conditions for ATR FT-IR measurements were a scan range of 400-4000 cm−1 with 32 scans, and a resolution of 4 cm−1. For the IR characterization of the LBDESs, a sample of the liquid has been examined as thin film, obtained by evaporation (under vacuum) of an aqueous solution (10 mg of LBDES in 2 mL of deionized water) deposited on a thallium bromide support.

Elemental analyses were performed on a Vario MICRO cube instrument (Elementar).

Thermogravimetric analyses were carried out using Mettler TGA Q500 thermogravimetric analyzer. Each sample (10 mg) was weighted and analyzed under nitrogen flux (60 ml/min). The selected heating speed was 10 °C/min from room temperature to 700 °C.

Conductivity measurements were carried out with VIO series 7 conductometer with integrated temperature probe. The measurements were conducted between 20°C and 70°C.

Density analysis was carried out with Anton Paar DMA 55 densimeter. The densimeter was calibrated with air and water with an error of ± 1x10-5 g/ml for samples which have a density from 0.5 to 1.5 g/ml. The measurements were conducted between 20 °C and 70 °C.

GLC-MS analyses were recorded with an Agilent 6890 N gas chromatograph interfaced with an Agilent MS5973 mass detector, using an Agilent J&W DB-5ms (30 m × 0.25 mm x 0.25 μm) column. UPLC-MS analyses were performed on an Acquity UPLC Water instrument (Phase A 95/5H2O/ACN+ 0.1% Formic Acid, Phase B 5/95H2O/ACN + 0.1% Formic Acid; Acquity UPLC 2.1 × 100 mm column, BEH C18, 1.7 μm; Flow 0.6 mL/min) coupled with an Acquity QDa Water mass spectrometer (Probe temperature: 600 °C; ESI capillary voltage 1.5V; Cone voltage 15V; Mass range 60–1000).

Viscosity measurements have not been carried out because of the corrosivity of the systems A and B toward steel. Anyway, comparing the flow rate with other DESs, the viscosity has been evaluated to be lower than 100 cP.

The number and weight average molecular weights (Mn, Mw) were determined by gel permeation chromatography (GPC), using a Jasco (Hachioji-shi, Tokyo, Japan) PU-2089 Plus liquid chromatograph equipped with two PL gel 5 µm mixed-D columns, a Jasco RI-2031 Plus refractive index detector, and a Jasco (Hachioji-shi, Tokyo, Japan) UV-2077 Plus UV/vis detector. Measurements were carried out using chloroform as the mobile phase, at a flux of 1 mL/min and a temperature of 30 °C maintained by a Jasco (Hachioji-shi, Tokyo, Japan) CO 2063 Plus column thermostat. Samples were filtered with a 0.2 µm PTFE filter before injection. Polystyrene standards were used for calibration. The refractive index detector was used to obtain reported values.

Differential scanning calorimetry (DSC) analysis was performed with a TA Instruments Discovery DSC model 250 under the nitrogen gas flow (50 mL min−1). Each sample (3-5 mg) was weighted and hermetically sealed into an aluminum DSC pan. A heating-cooling cycle from 25 to 300 °C at 10 °C/min, followed by a second heating scan in the same conditions was performed. The characteristic temperatures of PET samples were obtained from the second heating curve.

The degree of crystallinity was calculated using the following equation

Xc %= ∆Hm∆H°m∙100							(6)

where ΔHm is the melting enthalpy of PET sample and ΔH°m is the estimated specific melting enthalpy of the neat PET (140.1 J g−1). [47]

Inductively Coupled Plasma – Optical Emission Spectrometry (ICP–OES) analyses were performed on a Thermo Scientific iCAP 7200 Series ICP–OES instrument. Terephthalic acid before and after purification process was hydrolyzed using a mixture of HNO3/H2O2 (30%) 8:1 v/v in a microwave reactor for 30 minutes at 180 °C. The solution was diluted with Milli-Q water to obtain a final volume of at least 15 ml and analyzed by the instrument.

CRediT authorship contribution statement

Marco Rollo, Elisa Rossi: Investigation, Data curation. Francesca Raffi: Investigation. Matteo Tiecco, Elisa Martinelli, Gianluca Ciancaleoni: Supervision, Conceptualization, Formal Analysis.

Acknowledgements

This research is supported by the Ministry of University and Research (MUR) as part of the PON 2014-2020 “Research and Innovation” resources – Green/Innovation Action – DM MUR 1061/2022.

Declaration of Competing Interest

The authors declare that they have no known competing ﬁnancial interests or personal relationships that could have appeared to inﬂuence the work reported in this paper.

References

[1]	E. Barnard, J.J. Rubio Arias, W. Thielemans, Chemolytic depolymerisation of PET: A review, Green Chem. 23 (2021) 3765–3789. https://doi.org/10.1039/d1gc00887k.

[2]	Polyethylene Terephthalate Global Market Report 2022, (2022). https://www.thebusinessresearchcompany.com/report/polyethylene-terephthalate-global-market-report.

[3]	M. Crippa, B. Morico, PET depolymerization: A novel process for plastic waste chemical recycling, Stud. Surf. Sci. Catal. 179 (2019) 215–229. https://doi.org/10.1016/B978-0-444-64337-7.00012-4.

[4]	D. Paszun, T. Spychaj, Chemical Recycling of Poly(ethylene terephthalate), Ind. Eng. Chem. Res. 36 (1997) 1373–1383. https://doi.org/10.1021/ie960563c.

[5]	S. Kaabel, J.P. Daniel Therien, C.E. Deschênes, D. Duncan, T. Friščic, K. Auclair, Enzymatic depolymerization of highly crystalline polyethylene terephthalate enabled in moist-solid reaction mixtures, Proc. Natl. Acad. Sci. U. S. A. 118 (2021) e2026452118. https://doi.org/10.1073/pnas.2026452118.

[6]	T. Yoshioka, T. Sato, A. Okuwaki, Hydrolysis of waste PET by sulfuric acid at 150°C for a chemical recycling, J. Appl. Polym. Sci. 52 (1994) 1353–1355. https://doi.org/10.1002/app.1994.070520919.

[7]	J.J. Rubio Arias, W. Thielemans, Instantaneous hydrolysis of PET bottles: An efficient pathway for the chemical recycling of condensation polymers, Green Chem. 23 (2021) 9945–9956. https://doi.org/10.1039/d1gc02896k.

[8]	V.S. Zope, S. Mishra, Kinetics of neutral hydrolytic depolymerization of PET (Polyethylene terephthalate) waste at higher temperature and autogenious pressures, J. Appl. Polym. Sci. 110 (2008) 2179–2183. https://doi.org/10.1002/app.28190.

[9]	Q. Wang, X. Yao, S. Tang, X. Lu, X. Zhang, S. Zhang, Urea as an efficient and reusable catalyst for the glycolysis of poly(ethylene terephthalate) wastes and the role of hydrogen bond in this process, Green Chem. 14 (2012) 2559–2566. https://doi.org/10.1039/c2gc35696a.

[10]	Y. Wang, Y. Zhang, H. Song, Y. Wang, T. Deng, X. Hou, Zinc-catalyzed ester bond cleavage: Chemical degradation of polyethylene terephthalate, J. Clean. Prod. 208 (2019) 1469–1475. https://doi.org/10.1016/j.jclepro.2018.10.117.

[11]	T. Sako, T. Sugeta, K. Otake, N. Nakazawa, M. Sato, K. Namiki, M. Tsugumi, Depolymerization of polyethylene terephthalate to monomers with supercritical methanol, J. Chem. Eng. Japan. 30 (1997) 342–349. https://doi.org/10.1252/jcej.30.342.

[12]	P. Gupta, S. Bhandari, Chemical Depolymerization of PET Bottles via Ammonolysis and Aminolysis, in: S. Thomas, A. Rane, K. Kanny, A. V.K., M.G. Thomas (Eds.), Recycl. Polyethyl. Terephthalate Bottles, William Andrew Publishing, 2019: pp. 109–134. https://doi.org/10.1016/b978-0-12-811361-5.00006-7.

[13]	Z. Lei, B. Chen, Y.M. Koo, D.R. Macfarlane, Introduction: Ionic Liquids, Chem. Rev. 117 (2017) 6633–6635. https://doi.org/10.1021/acs.chemrev.7b00246.

[14]	Q.F. Yue, C.X. Wang, L.N. Zhang, Y. Ni, Y.X. Jin, Glycolysis of poly(ethylene terephthalate) (PET) using basic ionic liquids as catalysts, Polym. Degrad. Stab. 96 (2011) 399–403. https://doi.org/10.1016/j.polymdegradstab.2010.12.020.

[15]	S. Marullo, C. Rizzo, N.T. Dintcheva, F. D’Anna, Amino Acid-Based Cholinium Ionic Liquids as Sustainable Catalysts for PET Depolymerization, ACS Sustain. Chem. Eng. 9 (2021) 15157–15165. https://doi.org/10.1021/acssuschemeng.1c04060.

[16]	F. Liu, X. Cui, S. Yu, Z. Li, X. Ge, Hydrolysis reaction of poly(ethylene terephthalate) using ionic liquids as solvent and catalyst, J. Appl. Polym. Sci. 114 (2009) 3561–3565. https://doi.org/10.1002/app.30981.

[17]	Q. Wang, Y. Geng, X. Lu, S. Zhang, First-row transition metal-containing ionic liquids as highly active catalysts for the glycolysis of poly(ethylene terephthalate) (PET), ACS Sustain. Chem. Eng. 3 (2015) 340–348. https://doi.org/10.1021/sc5007522.

[18]	B.B. Hansen, S. Spittle, B. Chen, D. Poe, Y. Zhang, J.M. Klein, A. Horton, L. Adhikari, T. Zelovich, B.W. Doherty, B. Gurkan, E.J. Maginn, A. Ragauskas, M. Dadmun, T.A. Zawodzinski, G.A. Baker, M.E. Tuckerman, R.F. Savinell, J.R. Sangoro, Deep Eutectic Solvents: A Review of Fundamentals and Applications, Chem. Rev. 121 (2021) 1232–1285. https://doi.org/10.1021/acs.chemrev.0c00385.

[19]	Q. Wang, X. Yao, Y. Geng, Q. Zhou, X. Lu, S. Zhang, Deep eutectic solvents as highly active catalysts for the fast and mild glycolysis of poly(ethylene terephthalate)(PET), Green Chem. 17 (2015) 2473–2479. https://doi.org/10.1039/c4gc02401j.

[20]	E. Sert, E. Yılmaz, F.S. Atalay, Chemical Recycling of Polyethlylene Terephthalate by Glycolysis Using Deep Eutectic Solvents, J. Polym. Environ. 27 (2019) 2956–2962. https://doi.org/10.1007/s10924-019-01578-w.

[21]	O.A. Attallah, A. Janssens, M. Azeem, M.B. Fournet, Fast, High Monomer Yield from Post-consumer Polyethylene Terephthalate via Combined Microwave and Deep Eutectic Solvent Hydrolytic Depolymerization, ACS Sustain. Chem. Eng. 9 (2021) 17174–17185. https://doi.org/10.1021/acssuschemeng.1c07159.

[22]	R.M. Musale, S.R. Shukla, Deep eutectic solvent as effective catalyst for aminolysis of polyethylene terephthalate (PET) waste, Int. J. Plast. Technol. 20 (2016) 106–120. https://doi.org/10.1007/s12588-016-9134-7.

[23]	A. Paiva, A.A. Matias, A.R.C. Duarte, How do we drive deep eutectic systems towards an industrial reality?, Curr. Opin. Green Sustain. Chem. 11 (2018) 81–85. https://doi.org/10.1016/j.cogsc.2018.05.010.

[24]	Y. Liu, J.B. Friesen, J.B. McAlpine, D.C. Lankin, S.N. Chen, G.F. Pauli, Natural Deep Eutectic Solvents: Properties, Applications, and Perspectives, J. Nat. Prod. 81 (2018) 679–690. https://doi.org/10.1021/acs.jnatprod.7b00945.

[25]	Z. Yang, Toxicity and biodegradability of deep eutectic solvents and natural deep eutectic solvents, in: D.J. Ramón, G. Guillena (Eds.), Deep Eutectic Solvents Synth. Prop. Appl., Wiley-VCH Verlag GmbH & Co. KGaA, 2019: pp. 43–60. https://doi.org/10.1002/9783527818488.ch3.

[26]	H. Qin, X. Hu, J. Wang, H. Cheng, L. Chen, Z. Qi, Overview of acidic deep eutectic solvents on synthesis, properties and applications, Green Energy Environ. 5 (2020) 8–21. https://doi.org/10.1016/j.gee.2019.03.002.

[27]	M. Costamagna, E. Micheli, V. Canale, M. Ciulla, G. Siani, P. di Profio, M. Tiecco, G. Ciancaleoni, Low-cost temperature transition mixtures (TTM) based on ethylene glycol/potassium hydroxide as reversible CO2 sorbents, J. Mol. Liq. 340 (2021) 117180. https://doi.org/10.1016/j.molliq.2021.117180.

[28]	Y. Zhong, J. Wu, H. Kang, R. Liu, Choline hydroxide based deep eutectic solvent for dissolving cellulose†, Green Chem. 24 (2022) 2464–2475. https://doi.org/10.1039/d1gc04130d.

[29]	T. Yoshioka, T. Motoki, A. Okuwaki, Kinetics of hydrolysis of poly(ethylene terephthalate) powder in sulfuric acid by a modified shrinking-core model, Ind. Eng. Chem. Res. 40 (2001) 75–79. https://doi.org/10.1021/ie000592u.

[30]	X. Chen, H. Guo, A.A. Abdeltawab, Y. Guan, S.S. Al-Deyab, G. Yu, L. Yu, Brønsted-Lewis acidic ionic liquids and application in oxidative desulfurization of diesel fuel, Energy and Fuels. 29 (2015) 2998–3003. https://doi.org/10.1021/acs.energyfuels.5b00172.

[31]	S. Tao, L. Hu, X. Zhang, Y. Mai, X. Xian, X. Zheng, X. Lin, Insights into the Play of Novel Brønsted Acid-Based Deep Eutectic Solvents for the Conversion of Glucose into 5-Hydroxymethylfurfural without Additional Catalysts, Ind. Eng. Chem. Res. 61 (2022) 11645–11654. https://doi.org/10.1021/acs.iecr.2c01193.

[32]	Y. Bai, X.F. Zhang, Z. Wang, T. Zheng, J. Yao, Deep eutectic solvent with bifunctional Brønsted-Lewis acids for highly efficient lignocellulose fractionation, Bioresour. Technol. 347 (2022) 126723. https://doi.org/10.1016/j.biortech.2022.126723.

[33]	F. Liu, Z. Xue, X. Zhao, H. Mou, J. He, T. Mu, Catalytic deep eutectic solvents for highly efficient conversion of cellulose to gluconic acid with gluconic acid self-precipitation separation, Chem. Commun. 54 (2018) 6140–6143. https://doi.org/10.1039/c8cc03798a.

[34]	M.J. Kang, H.J. Yu, J. Jegal, H.S. Kim, H.G. Cha, Depolymerization of PET into terephthalic acid in neutral media catalyzed by the ZSM-5 acidic catalyst, Chem. Eng. J. 398 (2020) 125655. https://doi.org/10.1016/j.cej.2020.125655.

[35]	C.W. Song, J.W. Kim, I.J. Cho, S.Y. Lee, Metabolic Engineering of Escherichia coli for the Production of 3-Hydroxypropionic Acid and Malonic Acid through β-Alanine Route, ACS Synth. Biol. 5 (2016) 1256–1263. https://doi.org/10.1021/acssynbio.6b00007.

[36]	C. Lachaux, C.J.R. Frazao, F. Krauβer, N. Morin, T. Walther, J.M. François, A New Synthetic Pathway for the Bioproduction of Glycolic Acid From Lignocellulosic Sugars Aimed at Maximal Carbon Conservation, Front. Bioeng. Biotechnol. 7 (2019) 359. https://doi.org/10.3389/fbioe.2019.00359.

[37]	S.D. Mancini, M. Zanin, Post consumer pet depolymerization by acid hydrolysis, Polym. - Plast. Technol. Eng. 46 (2007) 135–144. https://doi.org/10.1080/03602550601152945.

[38]	N.R. Paliwal, A.K. Mungray, Ultrasound assisted alkaline hydrolysis of poly(ethylene terephthalate) in presence of phase transfer catalyst, Polym. Degrad. Stab. 98 (2013) 2094–2101. https://doi.org/10.1016/j.polymdegradstab.2013.06.030.

[39]	S. Mishra, A.S. Goje, V.S. Zope, Chemical recycling, kinetics, and thermodynamics of poly (ethylene terephthalate) (PET) waste powder by nitric acid hydrolysis, Polym. React. Eng. 11 (2003) 79–99. https://doi.org/10.1081/PRE-120018586.

[40]	D. Spaseska, M. Civkaroska, Alkaline hydrolysis of poly(ethylene terephthalate) recycled from the postconsumer soft-drink bottles, J. Univ. Chem. Technol. Met. 45 (2010) 379–384.

[41]	A. Căta, M.N. Ştefănuţ, I.M.C. Ienaşcu, C. Tănasie, M. Miclău, Alkaline hydrolysis of polyethylene terephthalate under microwave irradiation, Rev. Roum. Chim. 62 (2017) 531–538.

[42]	M.A.R. Martins, S.P. Pinho, J.A.P. Coutinho, Insights into the Nature of Eutectic and Deep Eutectic Mixtures, J. Solution Chem. 48 (2019) 962–982. https://doi.org/10.1007/s10953-018-0793-1.

[43]	J. González-Rivera, C. Pelosi, E. Pulidori, C. Duce, M.R. Tiné, G. Ciancaleoni, L. Bernazzani, Guidelines for a correct evaluation of Deep Eutectic Solvents thermal stability, Curr. Res. Green Sustain. Chem. 5 (2022) 100333. https://doi.org/10.1016/j.crgsc.2022.100333.

[44]	M.B. Taysun, E. Sert, F.S. Atalay, Physical properties of benzyl tri-methyl ammonium chloride based deep eutectic solvents and employment as catalyst, J. Mol. Liq. 223 (2016) 845–852. https://doi.org/10.1016/j.molliq.2016.07.148.

[45]	Y. Cui, C. Li, J. Yin, S. Li, Y. Jia, M. Bao, Design, synthesis and properties of acidic deep eutectic solvents based on choline chloride, J. Mol. Liq. 236 (2017) 338–343. https://doi.org/10.1016/j.molliq.2017.04.052.

[46]	N. Schaeffer, D.O. Abranches, L.P. Silva, M.A.R. Martins, P.J. Carvalho, O. Russina, A. Triolo, L. Paccou, Y. Guinet, A. Hedoux, J.A.P. Coutinho, Non-Ideality in Thymol + Menthol Type v Deep Eutectic Solvents, ACS Sustain. Chem. Eng. 9 (2021) 2203–2211. https://doi.org/10.1021/acssuschemeng.0c07874.

[47]	https://www.perkinelmer.com/Content/applicationnotes/app_thermalcrystallinitythermoplastics.pdf, (n.d.).