Vapochromic polyketone films based on aggregation induced enhanced emission

Giuseppe Iasilli,a Marco Scatto,b Andrea Puccia,c

aDipartimento di Chimica e Chimica Industriale, Università di Pisa, Via Giuseppe Moruzzi 13, 56124 Pisa, Italy 
bNadir S.r.l., c/o Campus Scientifico Università Ca’ Foscari Venezia, Via Torino 155b, 30172 Mestre (VE), Italy

cIstituto per i Processi Chimico-Fisici (IPCF), Consiglio Nazionale delle Ricerche, UOS Pisa, Via Giuseppe Moruzzi 1, 56124 Pisa, Italy

Corresponding author: Prof. Andrea Pucci, Dipartimento di Chimica e Chimica Industriale, Università di Pisa, Via Giuseppe Moruzzi 13, 56124 Pisa, Italy. Email: andrea.pucci@unipi.it

Abstract

Aliphatic polyketone (PK) films physically mixed with moderate amounts (0.6 wt.%) of 4,4’-bis(2-benzoxazolyl)stilbene (BBS) fluorophores were demonstrated to be sensitive to volatile organic compounds (VOCs). Notably, BBS/PK blends were prepared by means of a continuous one-step extrusion process in a pilot-scale twin screw extruder and compression moulded followed by rapid quenching in liquid nitrogen to get thin films (thickness of 150 µm) containing molecularly dispersed blue emissive BBS fluorophores.  The 0.6 wt.% BBS/PK films demonstrated significant vapochromism when exposed to VOCs characterized by favorable interactions with the polymer matrix such as chloroform. Solvent absorption caused PK matrix plasticization thus increasing BBS mobility and triggering the self-associations of molecules into bluish green-emissive excimers/aggregates thanks to the emersion of the typical band at 500 nm. This phenomenon preferentially involves the BBS/PK film layers close to the air-contact surface without affecting the bulk characteristics of the PK matrix. The easy modulation of the luminescent properties of PK films by varying the supramolecular organization of BBS dispersed molecules by chemical perturbations, and the use of melt-processing procedures suggests the use for the first time of aliphatic PK in the development of smart materials for sensing applications.

1. Introduction

The detection of Volatile Organic Compounds (VOCs) is a topic of great interest in various areas, including the monitoring of air quality and control of hazardous gases and vapours in industrial environments and workplaces.1, 2 In addition, pressing issues in global security are triggering the design of novel chromogenic compounds aimed at detecting environment changes with optical responses even more effective. For example, thermoplastic indicators containing fluorophore sensitive to viscosity changes have been used with success for the detection of VOCs.3-12 Notably, plastic films containing moderate amounts of the chromophoric probe (<0.1 wt.%) display fluorescence variations upon the exposure to well-interacting VOCs due to an induced plasticization of the continuous polymer phase.3-6, 9, 13 Plasticization means also viscosity decreasing, thus allowing the dispersed fluorophores to aggregate together upon a certain concentration threshold, which in turn causes evident colour changes. In this context, the 4,4’-bis(2-benzoxazolyl)stilbene (BBS) dye has been demonstrated to be an effective probe for the determination of polymer mechanical solicitations and thermal stress.14-21 BBS is typically employed as an optical brightener in several polymers thanks to its high compatibility, high resistance to solvent extraction and its very high melting point (360 °C) and degradation temperature (380 °C).22 Moreover, BBS molecules experience colour changes in emission due to the formation/disruption of excited dimes (excimers)23 as a function of external solicitations applied to the polymer matrix in which they are contained. Molecularly dispersed BBS emit intense blue light, whereas BBS excimers are characterized by a vivid green colour.

In this work, we have exploited the emission features of BBS molecules for the preparation of cost-effective plastic materials suitable for vapours detection. Semicrystalline aliphatic polyketone copolymers (PK, perfectly alternating copolymer of ethylene and carbon monoxide) was selected as supporting matrix since it exhibits many desirable thermoplastic properties, such as a high tensile yield stress and an excellent impact performance.24, 25 Moreover, its high degree of chemical resistance make this polymer interesting for future scale-up and engineered applications. In connection with these findings, we reported for the first time the preparation of vapochromic plastic indicators by means of a continuous one-step extrusion process in a pilot-scale intermeshing co-rotating twin screw extruder.

2. Experimental part

Materials

Aliphatic polyketone (PK, M630A, Melt Flow Index (g/10min 2.16Kg/240 °C) = 6, melting temperature = 222 °C supplied by Hyosung, South Korea) was used as polymer host matrix. 4,4’-Bis(2-benzoxazolyl)-stilbene (BBS, 97 %) was purchased from Aldrich and used without further purification.

Preparation of BBS/PK films

PK blends containing the 0.6 wt.% of BBS were prepared in a co-rotating twin screw extruder (THERMO, Polylab) with a screw diameter of 24 and a length-to-diameter of 40, introducing  about 966 g/h of polymers and 6 g/h of BBS. PK was extruded at fixed barrel temperature of 210 °C for first zone and 220 °C for following zones and with screw speed fixed at 80 rpm. The melt wire were taken at the die exit, solidified in a water bath and pelletized with a standard pelletizing machine. The recovered materials were grinded at room temperature by using an IKA MF10 analytical mill. The powder obtained was successively molded between two Teflon® foils under compression (max 4 atm) in a Collin-mod. 200M press at 260 °C for approximately 3 min and then rapidly quenched in liquid N2.

Characterizations

The thermal behaviour was evaluated by differential scanning calorimetry (DSC) under nitrogen atmosphere by using a Mettler Toledo StarE System, equipped with a DSC822c module. Blend samples were heated from -40 to 260 °C at 10 °C/min (1st heating), cooled to -40 °C at the same scan rate (1st cooling), then heated again to 260 °C at 10 °C/min (2nd heating). Melting enthalpies were evaluated from the integrated areas of melting peaks by using indium for calibration. PK crystalline content (χ) were evaluated from the measured melting enthalpy (ΔHm) taking into account the melting enthalpy of the perfect PK crystal (ΔH°m, 227 J/g), using equation 1:

χ=ΔHmΔH0∙100			(eq. 1)

The fluorescence measurements in the solid state were performed using a Horiba Jobin-Yvon Fluorolog®-3 spectrofluorometer equipped with a 450 W xenon arc lamp and double-grating excitation and single emission monochromators. The emission quantum yields of the solid samples were obtained by means of a 152 mm diameter "Quanta-phi" integrating sphere, coated with Spectralon®, using as excitation source the 450 W Xenon lamp coupled with a double-grating monochromator for selecting wavelengths.  Emission spectra of polymer films were recorded on the same spectrofluorometer in the dark by using a F-3000 Fibre Optic Mount apparatus (Horiba Jobin-Yvon) coupled with optical fibre bundles. Light generated from the excitation spectrometer is directly focused on the sample using optical fibre bundles. Emission from the sample is then directed back through the bundle into the collection port of the sample compartment. The emission response of the films towards vapours of volatile organic compounds (VOCs) was tested by exposing the sample held by a steel tripod in a 50 mL beaker closed by a pierced aluminium foil lid, to different concentrations of various organic solvents of different vapour pressure and interaction with PK.4, 5

3. Results and discussion

Semicrystalline aliphatic polyketones (PK) are insoluble in common organic solvents, and dissolve only in highly polar and acidic solvents such as hexafluoroisopropanol and m-cresol.26 Nevertheless, PK can be swelled in chloroform and in acetone only in part. Alcohols like methanol and ethanol do not affect PK features being completely uninteracting with the polymer matrix. For this reason, we investigated in this study the vapochromic features of BBS/PK films towards chloroform and acetone and the results compared with those using methanol as volatile organic compound (VOC). Aimed at preparing cost-effective optical devices, BBS was dispersed in PK in a co-rotating twin screw extruder and the derived blends containing the 0.6 wt.% of fluorophore were compressed molded to obtain films with a thickness of about 150 μm. Notably, the films were immediately quenched in liquid nitrogen in order to promote the very fine molecular dispersion of BBS dyes that resulted kinetically trapped within the PK matrix, thus avoiding the formation of excimers (Figure 1).15, 17, 18 Notably, the films appeared very well homogeneous, thus suggesting the very fine dispersion of the BBS fluorophores within the PK matrix. No evidences of macro- and micro-sized chromophoric assemblies were detected. This feature was conferred by the melt-processing technique being high temperature and shear stress beneficial to the additive phase dispersion.

|  | (a) |
| --- | --- |
|  | (b) |

Figure 1. a) Fluorescence of a 0.6 wt.% BBS/PK film after quenching in liquid nitrogen (λexc. = 366 nm); b) photograph of the same film (length = 2 cm) under the excitation of a long range UV lamp at 366 nm and the respective CIE 1931 chromaticity diagram

The emission spectrum of the film displays, when excited at 366 nm, an emission feature characterized by a well-defined vibronic structure attributed to the 0-0, 0-1 and 0-2 radiative transitions, pointed at 410, 440 and 475 nm, respectively (Figure 1a). Only a shoulder at higher wavelengths (around 500 nm) is detectable, thus suggesting the presence of negligible amounts of BBS aggregates within the quenched PK matrix. This is also confirmed by the typical purplish blue emission of uninteracting and molecularly dispersed BBS molecules (Figure 1b).14-16, 18, 27

The quenched film was then exposed to a saturated atmosphere of chloroform, acetone and methanol, respectively.

|  | (a) |
| --- | --- |
|  | (b) |

Figure 2. a) Fluorescence of a 0.6 wt.% BBS/PK film as a function of the exposure time of a saturated atmosphere of chloroform (λexc. = 366 nm, T = 25 °C). The spectra were collected for 90 minutes with an interval of 1 min; b) photograph of the same film (length = 2 cm) under the excitation of a long range UV lamp at 366 nm at the end of the experiment and the respective CIE 1931 chromaticity diagram

In figure 2, the fluorescence of the film is reported as a function of the exposure time of vapours of chloroform, i.e. the most interacting solvent with the PK matrix. Notably, the fluorescence spectra were normalized to the emission at 440 nm, i.e. that attributed to BBS molecularly dispersed fluorophores. It was worth noting that the quenched 0.6 wt.% BBS/PK film experienced an evident change of its emission features as soon as vapours of chloroform get in contact with the film surface (Figure 2a). Solvent adsorption and absorption caused polymer matrix plasticization thus increasing BBS mobility and triggering the self-associations of molecules into bluish green-emissive fluorogenic excimers/aggregates (Figure 2b). Notably, the band attributed to the supramolecular BBS assemblies progressively emerged at 500 nm and levelled-off that at 440 nm at the end of the experiment. The absolute quantum yield of BBS/PK film was found to be higher before solvent exposure, i.e. 39% against 29%, thus possibly suggesting that the concentration of BBS aggregates in the exposed films was greater than that of the remaining molecularly dispersed BBS. It is worth noting that the original features of the films can be infinitely restored by compression moulding followed by rapid quenching in liquid nitrogen, being the film components thermally stable within the experimental conditions.

The quenched 0.6 wt.% BBS/PK films were then exposed to a saturated atmosphere of acetone (Figure 3a) and methanol (Figure 3b), respectively, evaluated with the same conditions and time interval of 90 min.

|  | (a) |
| --- | --- |
|  | (b) |

Figure 3. Fluorescence of a 0.6 wt.% BBS/PK film as a function of the exposure time of a saturated atmosphere of a) acetone and b) methanol. In both cases, the spectra were collected for 90 minutes with an interval of 1 min (λexc. = 366 nm, T = 25 °C).

Figure 3 evidenced that the 0.6 wt.% BBS/PK film exposed to a saturated atmosphere of acetone experienced partial variation of the main emission features, showing a modest but detectable emersion of the band at 500 nm attributed to the formation of BBS luminescent aggregates. Conversely, this phenomenon was only minimal in the case of the film exposed to vapours of methanol, and it did not cause any substantial changes of the film emission colour.

The vapochromic behaviour of the 0.6 wt.% BBS/PK film was also quantitatively evaluated by calculating the ratio between the emission intensities at 500 nm (BBS aggregates) and at 440 nm (BBS monomers) as reported in Table 1.

Table 1. Variation of the I500/I440 ratio for pristine 0.6 wt.% BBS/PK films and after exposure of chloroform, acetone and methanol for the same time interval of 90 min.

|  | Pristine | Exposed to chloroform | Exposed to acetone | Exposed to methanol |
| --- | --- | --- | --- | --- |
| I500/I440 t = 0 min | 0.63 | 0.63 | 0.62 | 0.63 |
| I500/I440 t = 90 min | - | 0.98 | 0.89 | 0.76 |

As expected the 0.6 wt.% BBS/PK films displayed the greatest variation of the I500/I440 ratio in agreement with the evident colour changes reported in figure 1b. Acetone swells PK only in part and this behavior is reflected on the lower intensity ratio variation at the end of the exposure. In line with such reasoning, methanol barely affected the optical features of 0.6 wt.% BBS/PK films.

In order to give an insight on the thermal properties of the PK films, differential scanning calorimetry were performed before and after VOCs contamination (Figure 4).

Figure 4. First heating DSC scans of the investigated 0.6 wt.% BBS/PK blends and crystallinity degrees (in brackets).

As expected, the melting features of PK experiences strong variations upon quenching the film rapidly removed from the hot press in liquid nitrogen. The crystallinity degree changed from about 30 % to 25.5%. Notably, vapour exposure did not substantially affected the thermal behaviour of the films, even after chloroform exposure (curve not reported but crystallinity degree of 24.2%), thus suggesting that the vapochromic behaviour occurred only near the film surface without affecting the bulk of the material. Following such reasoning, vapours of well interacting solvent with PK such as chloroform are only able to swell the first layers near the film-air contact surface but this phenomenon results enough to increase the mobility of the close BBS molecules in forming enough amount of BBS aggregates.

4. Conclusions

We have demonstrated that aliphatic thermoplastic PK containing physically mixed with modest amount of BBS fluorophores (0.6 wt.%) can be suitable for the preparation of thin films with significant vapochromic features when vapours of well interacting solvents are utilized. The pronounced variation of the overall films fluorescence occurred within the first minutes of VOCs exposure was addressed to solvent-induced changes in the local viscosity of at the film air-contact surface. This phenomenon, in turn, promoted the emersion of the typical emission band at 500 nm attributed to the formation of emissive BBS excimers/aggregates. It was worth noting that chloroform produced the highest variation of the I500/I440 ratio, whereas acetone and eventually methanol displayed modest and meaningless changes of the overall emission features, respectively, owing to the lesser chemical interaction with the PK matrix.

All evidences therefore support the first time use of aliphatic PK as polymer matrix for the preparation of cost-effective, reusable thin films with smart sensing features such as a chromogenic behaviour towards external chemical solicitations. Future efforts will be devoted to select chromogenic fluorophores with aggregation induced emission (AIE)28-30 features aimed at increasing VOCs selectivity and sensibility threshold.

References

1	M. E. Jenkin, S. M. Saunders and M. J. Pilling, Atmospheric Environment 31:81-104 (1997).

2	Y. M. Kim, S. Harrad and R. M. Harrison, Environ Sci Technol 35:997-1004 (2001).

3	G. Martini, E. Martinelli, G. Ruggeri, G. Galli and A. Pucci, Dyes and Pigments 113:47-54 (2015).

4	G. Iasilli, F. Martini, P. Minei, G. Ruggeri and A. Pucci, Faraday Discussions 196:113-129 (2017).

5	M. Borelli, G. Iasilli, P. Minei and A. Pucci, Molecules 22:(2017).

6	P. Minei, M. Ahmad, V. Barone, G. Brancato, E. Passaglia, G. Bottari and A. Pucci, Polymers for Advanced Technologies 27:429-435 (2016).

7	T. Hayashi, A. Kobayashi, H. Ohara, M. Yoshida, T. Matsumoto, H.-C. Chang and M. Kato, Inorg Chem 54:8905-8913 (2015).

8	I. Platonova, A. Branchi, M. Lessi, G. Ruggeri, F. Bellina and A. Pucci, Dyes and Pigments 110:249-255 (2014).

9	P. Minei, M. Koenig, A. Battisti, M. Ahmad, V. Barone, T. Torres, D. M. Guldi, G. Brancato, G. Bottari and A. Pucci, Journal of Materials Chemistry C 2:9224-9232 (2014).

10	J. R. Kumpfer, S. D. Taylor, W. B. Connick and S. J. Rowan, J Mater Chem 22:14196-14204 (2012).

11	C. Elosua, C. Bariain, I. R. Matias, F. J. Arregui, E. Vergara and M. Laguna, Sens Actuators, B 137:139-146 (2009).

12	J. W. Grate, L. K. Moore, D. E. Janzen, D. J. Veltkamp, S. Kaganove, S. M. Drew and K. R. Mann, Chem Mater 14:1058-1066 (2002).

13	P. Minei and A. Pucci, Polymer International 65:609-620 (2016).

14	A. Battisti, P. Minei, A. Pucci and R. Bizzarri, Chemical Communications 53:248-251 (2017).

15	F. Martini, S. Borsacchi, M. Geppi, G. Ruggeri and A. Pucci, Polymer Chemistry 5:828-835 (2014).

16	A. Pucci, M. Bertoldo and S. Bronco, Macromolecular Rapid Communications 26:1043-1048 (2005).

17	A. Pucci, F. Di Cuia, F. Signori and G. Ruggeri, Journal of Materials Chemistry 17:783-790 (2007).

18	A. Pucci, F. Signori, R. Bizzarri, S. Bronco, G. Ruggeri and F. Ciardelli, J Mater Chem 20:5843-5852 (2010).

19	M. A. Fourati, C. Pellerin, C. G. Bazuin and R. E. Prud'homme, Polymer 54:730-736 (2013).

20	J. Kunzelman, T. Chung, P. T. Mather and C. Weder, J Mater Chem 18:1082-1086 (2008).

21	F. Ciardelli, G. Ruggeri and A. Pucci, Chem Soc Rev 42:857-870 (2013).

22	D. A. Jervis, Plast Addit Compd 5:42-46 (2003).

23	J. B. Birks, Reports on Progress in Physics 38:903-974 (1975).

24	G. A. Holt Jr and J. E. Spruiell, Journal of Applied Polymer Science 83:2124-2142 (2002).

25	J. M. Lagaron, M. E. Vickers, A. K. Powell and N. S. Davidson, Polymer 41:3011-3017 (2000).

26	D. Y. Goswam and F. Kreith, The CRC Handbook of Mechanical Engineering, CRC Press LLC, Boca Raton, FL, USA (2004).

27	F. Donati, A. Pucci, L. Boggioni, I. Tritto and G. Ruggeri, Macromol Chem Phys 210:728-735 (2009).

28	J. Mei, N. L. C. Leung, R. T. K. Kwok, J. W. Y. Lam and B. Z. Tang, Chemical Reviews 115:11718-11940 (2015).

29	J. Mei, Y. Hong, J. W. Y. Lam, A. Qin, Y. Tang and B. Z. Tang, Adv Mater 26:5429-5479 (2014).

30	R. Hu, N. L. C. Leung and B. Z. Tang, Chem Soc Rev 43:4494-4562 (2014).